文件编号/版次:GCL978/01                                                 发行日期:2005年6月15日

深 圳 市 一 通 达 焊 接 辅 料 有 限 公 司

产 品 资 料

1. 产品名称：

SMT贴片红胶ET-L978

2. 产品说明：

ET-L978贴片红胶，是单组份的环氧树脂胶粘剂。其高速长时间印刷仍可保持不拉丝、不溢胶、不塌陷的稳定形狀，其“剪切稀化＂粘度特性和低吸湿性，非常适合应用于常温厚网(铜网或胶网)印刷的 SMT工艺，胶点形狀非常容易控制，储存安定性好且具有优良的耐热冲击性和优良的电气特性，同时使用安全，不含溶剂，无气味，完全符合环保要求。

3. ET-L978贴片红胶特性（ Specification of ET-L978）

| 成 份 Composition | 环氧树脂： Epoxy resin |
| --- | --- |
| 外 观 Appearance | 红色糊状： Paste/red-colored |
| 比 重 Specific gravity | 1.31 |
| 粘 度 Viscosity at 25℃,5rpm | 350Pa·S |
| 摇变性指数 Thixotropy index | 6.8(1rpm/10rpm) |
| 接着强度Adhesive Strength 2125C Mini-mold tr SOP·IC16P 1206 0805 0603 0402 | 44N(4.5kgf)0.2mgr twin 45N(4.6kgf)0.3mgr twin 92N(9.4kgf)0.8mgf single×2 1.8KG 1.5KG 1.2KG 0.8KG |
| 电气特性 Electric Property 体积阻抗系数 Volume resistance 绝缘阻 Insulation resistance 初期值 Initial value 处理后* After treating* 介电常数 Dielectric constant 介电正接 Dielectric loss tangent | 3.6×1016Ω·cm JIS K6911 1.2×1014Ω JIS Z3197 1.2×1012Ω 3.12/1MHZ JIS K6911 0.012/1MHZ JIS K6911 |
| 保存条件 Preservation condition | 10℃以下的冰箱保存 To be strictly kept at less than 10℃ in refrigerator |

* 处理条件：85℃×85%RH×DC50V×1000hrs.    使用JIS Z3197梳型电极II型（G10）

*Treating condition:85℃×85%RH×DC50V×1000hrs.

*JIS Z3197 Measured at comb electrode model II (G10)

4.包装方式 （Package  styles）

| 包装方式 Package styles | 容量 Contents | 包装单位 Pack.Unit | 点胶机设备厂商 Applicable Dispenser Makers |
| --- | --- | --- | --- |
| 1．条装 Tube | 200gr | 10Pcs. | For all |
| 2．圆柱筒 | 300ml | 5Pcs. | For all |
| 3．圆柱筒 | 350gr | 12Pcs | For all |
| 4．罐装 PLASTIC JAR | 360gr | 12Pcs | For all |
| 5．罐装 PLASTIC JAR | 500gr | 10Pcs | For all |

5.特征（Features ）

| 1. Much lower temperature curing is aimed at amd is practically possible. 2. Very good stable curing shapes without stringing and slumping are achieved at super high speed dispensing and very amall dots. 3. stable adhesive strength can be obtained with a variety of SMD. 4. Long-term preservation stability is expected. 5. High heat-resistivity and excellent electric properties are possessed. 6. Usable for screen printing. | 1． 容许低温度硬化。 2． 尽管超高速涂敷、微少量涂敷仍可保持没有拉丝，塌陷的稳定形状。 3． 对於各种表面粘着零件，可获得安定的接着强度。 4． 储存安定性优良。 5． 具有高度耐热性和优良的电气特性。 6． 可用於网版印刷。 |
| --- | --- |

6.固化条件（Curing  condition）

| ○Recommended curing condition:Over 60 sec after PCB’s surface temperature has reached 150℃.or over 90 sec after PCB’s surface temperature has reached 120℃. ○When the higher curing temperature and the longer curing time,the stronger adhesive strength can obtained.We would suggest you to search out an optimum curing condition,for the temperature exerterd on the adhesive may occasionally vary according to the size,material,etc.of component parts mounted on PCBs. | 固化条件 ○建议固化条件是PCB板表面温度达到150℃后120秒以上 ○固化时间越长，可获得更高的粘接强度，依PCB板上装着元件材质、大小不同而实际附加于接着剂的温度会有所不同，因此请依据实际生产情况找出最适合的固化条件。 |
| --- | --- |

7.硬化条件曲线图（Example:curing profile）

160

150℃/120sec

140

120

100

80

60

40

20

90

120

30

60

210

240

150

180

270

300

8.使用方法（How  to  use）

| ○Adhesive should be preserved in refrigerator(below 5±3℃)to keep on its quality. ○Before processing,the adhesive should be taken out from the refrigerator for de-freezing about a few hours until it reaching the room temperature. ○The bottom of printing screen should be cleaned timely for good printing shape. ○Toluene or ethyl acetate is possible to use for cleaning up this adhesive. | 使用方法 ○为使接着剂的特性发挥最大效果，请务必放置于冰箱（5±3℃）保存。 ○使用前请务必提前4小时从冰箱取出，待红胶恢复至室温后使用。 ○为获得良好印刷成形，请及时清洁钢网底部。 ○对红胶的洗涤可使用甲苯，醋酸乙酯。 |
| --- | --- |

9.注意事项（Warning）

| ○Warranty:6Months. ○Store adhesive in a refrigerator keeping the temperature at 5±3℃ ○This product may cause skin irritation to sensitive personnel. ○In case Seal-glo ET-L978 gets in touch with skin,wash it thoroughly with soap and water. ○In case of eye contact,wash out with clean water and consult a medical doctor immediately. | ○保证期：6个月。 ○请务必将本品保存在5±3℃的冰箱内。 ○如果有过敏性体质的人，直接接触皮肤有时会引起皮肤过敏，因此请注意。 ○误沾皮肤时，请立即用肥皂水清洗。 ○进入眼睛时，请尽速以清水冲冼干净，立即接受医生的诊察。 |
| --- | --- |

10.备注（Remark）

本产品不宜在纯氧或富氧系统中使用。不可做为氯气或其它强氧化性物质的密封材料使用。有关本产品安全注意事项，请与一通焊接辅料技术部联系。冷藏储存的产品必须等到与室温（25℃±3℃）平衡后方可使用。使用之前应避免污染，沾在线路板上未固化的胶可用异丙醇等来擦掉。为了避免污染未用过的胶液，不可将任何胶装回原来的包装容器内。本文中的数据是根据实际的测试数据和周期性试验取得的，仅供客户参考，对于任何人采用我们无法控制的方法得到的结果，我们恕不负责。决定把本产品用于哪一种生产方法，及采取用哪一种措施来防止产品在贮存和使用过种中可能发生的损身和人身伤害都是客户自已的责任。建议客户每次在正式使用之前都要根据本文所提供的数据先做试验。