Designation: D 1709 – 04

Standard Test Methods for

Impact Resistance of Plastic Film by the Free-Falling Dart

Method1

This standard is issued under the ﬁxed designation D 1709; the number immediately following the designation indicates the year of

original adoption or, in the case of revision, the year of last revision. A number in parentheses indicates the year of last reapproval. A

superscript epsilon (e) indicates an editorial change since the last revision or reapproval.

1. Scope*

1.1 These test methods cover the determination of the

energy that causes plastic ﬁlm to fail under speciﬁed conditions

of impact of a free-falling dart. This energy is expressed in

terms of the weight (mass) of the missile falling from a

speciﬁed height which would result in 50 % failure of speci-

mens tested.

1.2 Two test methods are described:

1.2.1 Test Method A employs a dart with a 38.10 6 0.13-

mm [1.500 6 0.005-in.] diameter hemispherical head dropped

from a height of 0.66 6 0.01 m [26.0 6 0.4 in.]. This test

method may be used for ﬁlms whose impact resistances require

masses of about 50 g or less to about 2 kg to fracture them.

1.2.2 Test Method B employs a dart with a 50.80 6 0.13-

mm [2.000 6 0.005-in.] diameter hemispherical head dropped

from a height of 1.50 6 0.03 m [60.0 + 0.25, −1.70 in.]. Its

range of applicability is from about 0.3 kg to about 2 kg.

1.3 Two testing techniques are described:

1.3.1 The standard technique is the staircase method. By

this technique, a uniform missile weight increment is employed

during test and the missile weight is decreased or increased by

the uniform increment after test of each specimen, depending

upon the result (fail or not fail) observed for the specimen.

1.3.2 The alternative technique provides for testing speci-

mens in successive groups of ten. One missile weight is

employed for each group and missile weight is varied in

uniform increments from group to group.

1.3.3 The staircase technique and the alternative technique

give equivalent results both as to the values of impact failure

weight which are obtained and as to the precisions with which

they are determined.

1.4 The values stated in SI units are to be regarded as

standard. The values stated in parentheses are for information

only.

NOTE 1—Tests on materials that do not break, for any reason, are not

considered to be valid. It has been noted that certain materials may stretch

so far as to bottom out at the base of certain test instruments without

actually rupturing. Subcommittee D20.19 is currently considering meth-

ods for testing these materials. Anyone interested in participating in a Task

Group should contact the Chairman of Subcommittee D20.19 through

ASTM International Headquarters.

NOTE 2—This test method is technically equivalent to ISO 7765-1:

1988, with the exception of a larger tolerance on the drop height in Test

Method B. Also, the ISO method does not allow the alternative testing

technique described in Section 11 of this test method.

1.5 This standard does not purport to address the safety

concerns, if any, associated with its use. It is the responsibility

of the user of this standard to establish appropriate safety and

health practices and determine the applicability of regulatory

limitations prior to use.

2. Referenced Documents

2.1 ASTM Standards: 2

D 374 Test Methods for Thickness of Solid Electrical Insu-

lation

D 618 Practice for Conditioning Plastics for Testing

D 883 Terminology Relating to Plastics

D 1248 Speciﬁcation for Polyethylene Plastics Extrusion

Materials for Wire and Cable

D 3420 Test Method for Dynamic Ball Burst (Pendulum)

Impact Resistance of Plastic Film

D 4272 Test Method for Total Energy Impact of Plastic

Films by Dart Drop

E 177 Practice for Use of the Terms Precision and Bias in

ASTM Test Methods

E 691 Practice for Conducting an Interlaboratory Study to

Determine the Precision of a Test Method

2.2 ISO Standard:

ISO 7765:1988 Plastic Film and Sheeting—Determination

of Impact Resistance by the Free Falling Dart Method—

Part 1: Staircase Method3

3. Terminology

3.1 Deﬁnitions—For deﬁnitions related to plastics, see

Terminology D 883.

For referenced ASTM standards, visit the ASTM website, www.astm.org, or

contact ASTM Customer Service at service@astm.org. For Annual Book of ASTM

Standards volume information, refer to the standard’s Document Summary page on

the ASTM website.

3Available from American National Standards Institute (ANSI), 25 W. 43rd St.,

4th Floor, New York, NY 10036.

2

These test methods are under the jurisdiction of ASTM Committee D20 on

Plastics and are the direct responsibility of Subcommittee D20.19 on Film and

Sheeting.

Current edition approved October 1, 2004. Published October 2004. Originally

approved in 1959. Last previous edition approved in 2003 as D 1709 – 03.

1

*A Summary of Changes section appears at the end of this standard.

Copyright © ASTM International, 100 Barr Harbor Drive, PO Box C700, West Conshohocken, PA 19428-2959, United States.

1

www.bzxzw.com

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

3.2 Deﬁnitions of Terms Speciﬁc to This Standard:

3.2.1 failure—any break through the ﬁlm that can be ob-

served readily by feeling or by viewing the specimen under

backlighted condition.

3.2.2 impact failure weight—that missile weight, estimated

statistically, at which 50 % of the specimens would fail in the

speciﬁed test.

3.2.3 missile weight—the weight (mass) of the dart plus the

total value of incremental weights attached plus the locking

collar.

4. Signiﬁcance and Use

4.1 Test Methods A and B are used to establish the weight of

the dart when 50 % of the specimens fail under the conditions

speciﬁed. Data obtained by one test method cannot be com-

pared directly with the other test method nor with those

obtained from tests employing different conditions of missile

velocity, impinging surface diameter, effective specimen diam-

eter, and thickness. The values obtained by these test variables

are highly dependent on the method of ﬁlm fabrication.

4.2 The results obtained by Test Methods A and B are

greatly inﬂuenced by the quality of ﬁlm under test. The

conﬁdence limits of data obtained by this procedure can,

therefore, vary signiﬁcantly, depending on the sample quality,

uniformity of ﬁlm gage, die marks, contaminants, etc. (see

Section 15).

4.3 Test Methods A and B have been found useful for

speciﬁcation purposes. Correlation between test results and

ﬁeld performance can usually be established.

4.4 The impact resistance of plastic ﬁlm, while partly

dependent on thickness, has no simple correlation with sample

thickness. Hence, impact values cannot be normalized over a

range of thickness without producing misleading data as to the

actual impact resistance of the material. Data from these test

methods are comparable only for specimens that vary by no

more than 625 % from the nominal or average thickness of the

specimens tested.

4.5 Several impact test methods are used for ﬁlm. It is

sometimes desirable to know the relationships among test

results derived by different test methods. A study was con-

ducted in which four ﬁlms made from two resins (polypropy-

lene and linear low-density polyethylene), with two ﬁlm

thicknesses for each resin, were impacted using Test Methods

D 1709 (Method A), D 3420 (Procedures A and B), and

D 4272. The test results are shown in the Appendix. Differ-

ences in results between Test Methods D 1709 and D 4272 may

be expected since Test Methods D 1709 represents failure

initiated energy, while Test Method D 4272 is initiation plus

completion energy. Some ﬁlms may show consistency when

the initiation energy is the same as the total energy. This

statement and the test data also appear in the signiﬁcance

sections and appendixes of Test Methods D 3420 and D 4272.

5. Apparatus

5.1 The apparatus shall be constructed essentially as shown

in Fig. 1, using the following components common to both test

methods:

2

5.1.1 Dart Well—If the dart impact machine utilizes an

enclosed dart well, it must contain a single unobstructed vent

with a minimum area of 625 mm2 (~1 in.2) to provide adequate

venting.

NOTE 3—Some dart impact machine designs utilize enclosed dart wells

that do not permit adequate venting to the atmosphere during impact. Data

have shown that this has a signiﬁcant effect on the observed impact value,

especially with ﬁlms that exhibit high elongation during testing, resulting

in atypically high impact values.

NOTE 4—The use of smaller, multiple vents is permitted if it can be

demonstrated that the venting efficiency is comparable and has no

statistically signiﬁcant effect on the values obtained.

5.1.2 Specimen Clamp—A two-piece annular specimen

clamp having an inside diameter of 125 6 2.0 mm [5.0 + 0.0,

−0.15 in.] and conforming to the following requirements:

5.1.2.1 The lower or stationary half of the clamp shall be

mounted rigidly so that the plane of the specimen is horizontal.

5.1.2.2 The upper or movable part of the clamp shall be

designed to maintain positive and plane contact with the lower

part of the clamp when in position. The clamps shall be

provided with suitable means of maintaining sufficient contact

to hold the ﬁlm sample ﬁrmly in place during the test.

Pneumatically operated clamps have been successfully em-

ployed.

5.1.2.3 Rubber-like gaskets may be affixed to the specimen

contact surfaces of both clamps to provide a cushion which

minimizes thickness variation effects. Rubber gasketing

3.0 6 1 mm [0.125 + 0.025, −0.04 in.] thick, of 50 to 60 Shore

A durometer hardness, 125 6 2.0 mm [5.00 + 0.00, −0.15 in.]

in inside diameter and 150 6 3.0 mm [6.0 + 0.02, −0.2 in.] in

outside diameter has been found satisfactory for this purpose.

5.1.2.4 Slippage of ﬁlms greater than 0.10 mm [0.004 in.] in

thickness may be minimized or eliminated by securing crocus

cloth or 50D garnet abrasive paper to the gaskets with double

sensitive tape so that the abrasive surface is in direct contact

with the ﬁlm. There should be sufficient clamping force to

eliminate detectable slippage. Other means of reducing slip-

page such as additional clamping devices or positive clamping

surfaces may be used provided that the ﬁlm is not weakened at

the inside wall of the specimen clamps and that the effective

diameter of 125 6 2.0 mm [5.00 + 0.00, −0.15 in.] of the ﬁlm

is not changed.

5.1.3 Dart Release Mechanism, capable of supporting a

2-kg weight shall be used for supporting and releasing the dart

assembly. It shall be equipped with a centering device, such as

a removable plumb bob, to ensure a reproducible drop. Either

an electromagnetic- or pneumatic-operated release mechanism

may be used.

5.1.4 Positioning Device—The apparatus shall be able to

drop the dart from heights of 0.66 6 0.01 m [26.0 6 0.4 in.]

for Test Method A and 1.50 6 0.03 m [60.0 + 0.25, −1.70 in.]

for Test Method B. The distance between the impinging surface

of the dart head and the surface of the test specimen is

considered to be the drop height. The dart shall be positioned

vertically above the center of the test specimen.

5.1.5 Micrometer, accurate to 60.0025 mm [60.0001 in.]

in the range from 0.0025 mm [0.0001 in.] to 1 mm [0.4 in.] for

measuring specimen thickness (see Test Methods D 374).

www.bzxzw.com

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

NOTE 1—Values for tolerances in SI units are to be regarded as standard. The numbers in parentheses reﬂect the allowable tolerance range of older

equipment and are only provided for information and, in many cases, do not correspond directly to the tolerances in SI units. The differences are not

expected to have a signiﬁcant effect on the results but the dimensions in SI units shall be used in cases of dispute.

NOTE 2—Legend Dart Assembly:

A. Steel shaft tip 6.5 6 1 mm [0.25 + 0.04, −0.03 in.] OD by 12.5 6 0.2 mm [0.50 + 0.00, −0.02 in.] long.

B. Dart shaft: 6.5 6 1 mm [0.25 + 0.04, −0.03 in.] OD and at least 115 mm [4.5 in.] long: 1⁄4 –20 thd. (N.C.) 12.5 6 0.2 mm [0.50 + 0.00, −0.02 in.]

long on bottom: No. 5–40 thd. (N.F.) for steel tip.

C. Hemispherical head: Method A—38.10 6 0.13–mm [1.500 6 0.005–in.] in diameter. Method B—50.80 6 0.13–mm [2.000 6 0.005 in.] in diameter.

D. Removable weights.

E. Collar and screw.

FIG. 1 Apparatus for Free-Falling Dart Impact Test for Plastic Film

5.1.6 Cushioning and Shielding Devices, to protect person-

nel and to avoid damaging the impinging surface of the dart.

These devices shall not interfere with the dart or the specimen

prior to penetrating the specimen.

5.1.7 Collar with inside diameter of approximately 7 mm

[0.28 in.] and with set screw for securing collar to dart shaft.

5.2 Darts for Test Methods A and B shall have hemispheri-

cal heads, each ﬁtted with a 6.5 6 1-mm [0.25 + 0.04, −0.03-

in.] diameter shaft at least 115 mm [4.5 in.] long to accommo-

date removable incremental weights. Each dart weight shall be

known to 60.5 % relative. Dart head surfaces shall be free of

nicks, scratches, or other irregularities. The shaft shall be

attached to the center of the ﬂat surface of the head with its

longitudinal axis perpendicular to the surface. If an electro-

magnet is used, the shaft shall be made of material that is not

magnetic and shall have a steel tip 125 6 0.2 mm [0.50 + 0.00,

−0.02 in.] long at the end held by the electromagnet.

5.2.1 For Test Method A, the dart head shall be

38.10 6 0.13–mm [1.500 6 0.005–in.] in diameter. It may be

constructed of smooth, polished aluminum, phenolic, or other

low-density material of similar hardness.

5.2.2 For Test Method B, the dart head shall be

50.80 6 0.13–mm [2.000 6 0.005 in.] in diameter. It may be

constructed of smooth, polished stainless steel or other material

of similar durability.

3

www.bzxzw.com

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

5.3 The material of construction of the dart head shall be

referenced in the report using the following designations:

Material Construction

Stainless Steel

Aluminum

Phenolic

Composite

Other

Designation

A

B

C

D

E

NOTE 5—Data have shown a sensitivity of impact results related to the

material of construction and ﬁnish of the dart head used. The differences

have been especially signiﬁcant when testing ﬁlms exhibiting high impact,

or high elongation characteristics, or both. This issue, together with related

concerns, is currently under study in Subcommittee D20.19.

less than 40 h prior to test in accordance with Procedure A of

Practice D 618, for those tests where conditioning is required.

In cases of disagreement, the tolerances shall be 61°C

[61.8°F] and 62 % relative humidity.

7.2 Test Conditions—Conduct tests in the standard labora-

tory atmosphere of 23 6 2°C [73.4 6 3.6°F] and 50 6 5 %

relative humidity unless otherwise speciﬁed in the materials

speciﬁcation. In cases of disagreement, the tolerances shall be

61°C [61.8°F] and 62 % relative humidity.

8. Preparation of Apparatus

8.1 Set up the apparatus for testing by Test Method A or by

Test Method B.

8.1.1 For Test Method A select a dart with a 38.10 6 0.13-

mm [1.500 6 0.005-in.] diameter hemispherical head. For Test

Method B, select a dart with a 50.80 6 0.13-mm

[2.000 6 0.005-in.] diameter hemispherical head.

8.1.2 Activate the dart release mechanism and insert the

steel shaft tip into the mechanism. The dart should be held in

place by the dart release mechanism. Adjust the drop height

(the vertical distance from the plane of a clamped specimen to

the bottom surface of the dart head) to 0.66 6 0.01 m

[26.0 6 0.4 in.] for Test Method A or to 1.50 6 0.03 m

[60.0 + 0.25, −1.70 in.] for Test Method B. (Warning—For

safety reasons, remove the dart while making position adjust-

ments.)

8.1.3 With a trial ﬁlm specimen clamped between the

specimen clamps and with no added weights on the dart,

release the dart and observe the point at which the dart impacts

the specimen, catching the dart after it bounces off the ﬁlm

surface. If necessary, adjust the dart release mechanism so that,

in repeated trials, the dart reproducibly impacts the center of

the clamped portion of the ﬁlm.

8.2 Check the apparatus periodically to make sure specimen

slippage during testing is not occurring. If slippage occurs, this

is reason to reject the results. The likelihood of occurrence of

slippage increases with increasing dart weight and with in-

creasing drop height and is greater with some materials than

with others. Slippage may be checked conveniently during the

course of testing of a routine sample at a missile weight

wherein both failures and non-failures are being observed.

Either of the following procedures is effective.

8.2.1 Before dropping the missile on a clamped specimen,

draw a circle on the ﬁlm using a ball-point pen in contact with

the inside wall of the upper clamp. Apply only the pressure of

the pen itself to the ﬁlm. After the dart is dropped and prior to

removing the plastic ﬁlm, draw another circle using a ball-

point pen of another color. If the lines are drawn, distinct

double lines at any point on the circumference show that

slippage has occurred. (Warning—For safety reasons, the dart

should not be in the dart release mechanism while drawing the

circle.)

8.2.2 If crocus cloth or sandpaper is affixed to the gaskets to

effect greater gripping, determine slippage simply by inspect-

ing the clamped ﬁlm area after impact for evidence of scratch

marks produced as slippage occurred.

4

5.4 Incremental Weights for Test Methods A and B shall be

of stainless steel or brass and cylindrical in shape. Each shall

have a center hole 6.6 + 1.0, −0.00 mm [0.26 + 0.03, −0.00 in.]

in diameter. The thickness of each shall be adjusted to obtain

the speciﬁed weight within 60.5 %. The diameter of the

weights shall not exceed the diameter of the dart head.

Suggested combination of weights for the speciﬁed diameters

are as follows:

5.4.1 For Test Method A, 31.5 6 1-mm [1.25 + 0.03, −0.05-

in.] diameter weights.

Number

2 or more

8

8

8

Weight, g

5

15

30

60

5.4.2 For Test Method B, 45.0 6 1-mm [1.75 + 0.06, −0.02-

in.] diameter weights.

Number

2 or more

8

8

Weight, g

15

45

90

5.4.3 Optionally, additional weights, each 120 g 6 0.5 %

for Test Method A or 180 g 6 0.5 % for Test Method B, may

be constructed for use if it is necessary to extend the missile

weight beyond that attainable when using all weights in the

standard set.

6. Test Specimen

6.1 Test specimens shall be large enough to extend outside

the specimen clamp gaskets at all points. The specimens shall

be representative of the ﬁlm under study and shall be taken

from the sheet or tube in a manner representative of sound

sampling practice. This is to ensure that the whole of the sheet

be represented in the test unless such sampling constitutes a

variable under study.

6.2 The specimens shall be free of pinholes, wrinkles, folds,

or other obvious imperfections, unless such imperfections

constitute variables under study.

7. Conditioning

7.1 Conditioning—Follow the conditioning requirements

speciﬁed in the materials speciﬁcation for the material that is

being tested. Otherwise, condition the test specimens at

23 6 2°C [70 to 77°F] and 50 6 5 % relative humidity for not

www.bzxzw.com

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

STAIRCASE TESTING TECHNIQUE

9. Procedure

9.1 By this technique, a uniform missile weight increment is

employed during test and the missile weight is changed after

test of each specimen.

9.2 Select Test Method A or Test Method B for use, as

desired, or as required by the relevant material speciﬁcation.

Set up the apparatus for testing as described in 8.1. If desired,

carry out a slippage check as described in 8.2 at some point

during the course of testing.

9.3 Measure and record the average thickness of the test

specimens in the area of impact to the nearest 0.0025 mm

[0.0001 in.].

9.4 For a starting point, select a missile weight near the

expected impact failure weight. Add the necessary number of

incremental weights onto the dart shaft and put the locking

collar into place so that the weights are held securely in place.

9.5 Select a missile weight increment DW appropriate to the

impact strength of the sample: The value chosen for DW should

be such that three to six (but at least three) missile weights will

be employed in the determination. A DW value equal to some

5 to 15 % of WF, the impact failure weight, is usually

appropriate.

9.6 Place the ﬁrst test specimen over the bottom part of the

clamp, making sure that it is uniformly ﬂat, free of folds, and

that it covers the gasket at all points. Clamp in place with the

top part of the annular clamp.

9.7 Activate the dart release mechanism and put the dart

into position. Release the dart. If the dart bounces off the

specimen surface, catch the dart after it bounces to prevent

both multiple impact with the specimen surface and damage to

the hemispherical contact surface of the dart resulting from

impact with metal parts of the apparatus.

9.8 Examine the test specimen for any evidence of slippage.

If slippage occurs, this is reason to reject the results.

9.9 Examine the specimen to determine whether it has or

has not failed. Record the result on a form such as that shown

in Fig. 2, using a 0 to denote non-failure and an X to denote

failure, or any other similar convention to indicate non-failure

or failure.

9.10 If the ﬁrst specimen failed, decrease the missile weight

by DW. If the ﬁrst specimen did not fail, increase the missile

weight by DW. Test the second specimen. Continue testing

successive specimens, decreasing or increasing the missile

weight by DW between drops depending upon whether the

preceding specimen did or did not fail.

9.11 After 20 specimens have been tested, count the total

number, N, of failures, (X’s). If N = 10 at this point, testing is

complete. If not, complete testing as follows:

9.11.1 If N < 10, continue testing additional specimens until

N = 10, then stop testing.

NOTE—

WF 5 Wo 1 [DW ~A/N 2 1/2!#

5 120 1 [15~15/10 2 1/2!#

5 120 1 [15~1.5 2 0.5!#

5 135 g.

FIG. 2 Determination of Dart Impact Failure Weight

5

www.bzxzw.com

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

9.11.2 If N > 10, continue testing additional specimens until

the total number of non-failures (0’s) reaches 10, then stop

testing.

10. Calculation

10.1 On the data record-calculation form (see Fig. 2), record

under ni the total number of X’s at each missile weight,

counting only the last 10 X’s during test.

NOTE 6—If, during test, after 20 drops, N < 10 or N = 10, there will be

only 10 X’s after testing is complete. Only where N > 10 after 20 drops

will it be necessary to omit some of the earlier X results.

10.2 Under i, enter integers 0, 1, 2, etc. for each ni entry.

Enter 0 for the lowest missile weight at which an ni value has

been entered, a 1 for next higher missile weight, etc.

10.3 Under ini, enter the product of i times ni.

10.4 Add the ni’s and enter as N; by the procedure de-

scribed, N will always be 10. Add the ini’s and enter as A. Enter

Wo, the missile weight to which an i value of zero is assigned.

Enter DW the uniform missile weight increment employed.

10.5 Calculate the impact failure weight WF, g, as follows:

WF 5 Wo 1 [DW ~A/N 2 1/2!#

that it covers the gasket at all points. Clamp in place with the

top part of the annular clamp.

11.6 Activate the dart release mechanism and put the dart

into position. Release the dart. If the dart bounces off the

specimen surface, catch the dart after it bounces to prevent

both multiple impact with the specimen surface and damage to

the hemispherical contact surface of the dart resulting from

impact with metal parts of the apparatus.

11.7 Test a total of ten specimens at the selected starting

missile weight. Record the missile weight and the percentage

of failures.

11.8 If the failure result for the ﬁrst group of ten specimens

is 0 or 100 %, increase or decrease the missile weight by 15 g

or more for Test Method A or 45 g or more for Test Method B

and test another ten specimens as previously described. Con-

tinue in this manner until a failure result between 0 and 100 %

is obtained. Continue testing groups of ten specimens, varying

the missile weight between tests by the selected uniform

increment, until results encompassing the entire range from 0

to 100 % failure inclusive have been obtained.

NOTE 8—For efficiency in testing, it is suggested that the missile weight

increment selected initially be relatively large so that 0 and 100 % failure

results will be found after testing only two or three groups of specimens.

“Fill-in” results between the corresponding extremes of missile weight can

then be obtained in subsequent testing.

ALTERNATIVE TESTING TECHNIQUE

11. Procedure

11.1 By this technique, successive groups of ten specimens

each are tested. For each group, one missile weight is em-

ployed and from group to group missile weight is varied in

uniform increments. Testing is carried to a point where there

are at least ﬁve results for percentage failure: one 0 % result,

one 100 % result and at least three results between 0 and

100 %.

NOTE 7—In quality control work, one may ﬁnd it useful to estimate WF

from fewer than ﬁve failure results at missile weights not necessarily

uniformly spaced. Of these, no result should be 0 or 100 % failure, at least

one result should be less than 50 %, and at least one result should be

greater than 50 %. Either the individual results or moving averages-of-two

are plotted on probability paper (see 12.4), a straight line is ﬁtted, and WF

is read from the plot. Values of WF estimated in this manner will be

unbiased but will not be as precise as values derived from at least ﬁve

failure results employing uniform missile weight increments as previously

described.

11.9 At this stage, if the minimum ﬁve results described in

11.1 have been obtained, testing is complete. If not, select a

new missile weight increment less than that employed initially.

Test additional groups of specimens as previously described

beginning at one weight increment below the lowest missile

weight at which 100 % failure occurred. Continue testing

specimen groups at increasingly lower missile weights employ-

ing the new uniform increment, until a result of 0 % failure is

obtained (note that one or more of the percentage points found

in 11.8 may be usable in this series employing a smaller weight

increment). If the minimum ﬁve results have now been

obtained, testing is complete. If not, select a still smaller

weight increment and repeat the preceding process, continuing

in this manner until the minimum ﬁve results at uniform weight

increments have been obtained.

12. Calculation

12.1 Determine impact failure weight, WF, by calculation as

described in 12.2 or by graphing as described in 12.4. These

two approaches give essentially the same results.

12.2 Calculate WF as follows:

WF 5 WL 2 [DW ~S/100 2 1/2!#

11.2 Select Test Method A or Test Method B for use, as

desired, or as required by the relevant material speciﬁcation.

Set up the apparatus for testing in accordance with 8.1. If

desired, carry out a slippage check as described in 8.2 at some

point during the course of testing.

11.3 Measure and record the average thickness of the test

specimens in the area of impact to the nearest 0.0025 mm

[0.0001 in.].

11.4 For a starting point, select a missile weight near the

expected impact failure weight. Add the necessary number of

incremental weights onto the dart shaft and put the locking

collar into place so that the weights are held securely in place.

11.5 Place the ﬁrst test specimen over the bottom part of the

clamp, making sure that it is uniformly ﬂat, free of folds, and

where:

WF = impact failure weight, g,

DW = uniform weight increment used, g,

WL = lowest missile weight, g, according to the particular

DW used, at which 100 % failure occurred, and

S= sum of the percentages of breaks at each missile

weight (from a weight corresponding to no failures

up to and including WL).

6

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

12.3 Example of calculation:

Given:

Missile Weight, g

91

106

121

136

151

% Failure

0

10

20

60

100

S = 190

determined by calculation by 12.2 are (1) 138, (2) 117, and (3)

92 g.

13. Routine Inspection and Acceptance

13.1 For routine inspection of thin plastic ﬁlm of a speciﬁed

gage received from an approved supplier, it shall be satisfac-

tory to accept lots on the basis of testing a minimum of ten

specimens at a speciﬁed weight as stated in the relevant

material speciﬁcation. Under this procedure, a result of no

more than ﬁve failures shall be acceptable.

14. Report

14.1 Report the following information:

14.1.1 Complete identiﬁcation and description of the mate-

rial tested, including type, source, manufacturer’s code, prin-

cipal dimensions, and previous history.

14.1.2 Impact failure weight, to the nearest 1 g,

14.1.3 Method used,

14.1.4 Designation of dart head material,

14.1.5 Thickness of ﬁlm tested and range of thickness for

specimens tested,

14.1.6 Conditioning procedure followed,

14.1.7 Testing technique used, and

14.1.8 Date of test.

DW = 15 g, WL = 151 g

WF = WL − [DW (S/100 − 1/2)]

= 151 − [15(190/100 − 1/2)]

= 151 − [15(1.4)]

= 130 g

12.4 Average successive pairs of missile weight-percent

failure results, including 0 % and 100 % failure points, to

obtain points for plotting. Construct a plot on probability paper

with percent failure on the probability scale and weight on the

linear scale after having dimensioned the linear scale such that

the resultant straight line deﬁned by the points will have a slope

between about 0.3 and 1.0. Draw the best ﬁtting straight line

through the points and read WF from the graph as that missile

weight corresponding to the intersection of the straight line

with the 50 % probability line.

12.5 Examples of the graphical method for determining WF

are given in Fig. 3. For the three cases shown, values of WF

FIG. 3 Graphical Determination of Impact Failure Weight

7

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

14.2 For routine inspection and acceptance testing only

(13.1) the following shall be reported, instead of items 14.1.2

and 14.1.6:

14.2.1 Weight used, and

14.2.2 Number of failures.

15. Precision and Bias4

TABLE 1 Drop Dart Impact Data F-50

NOTE—Values expressed in units of grams

Material

Commercial Polyethylene

Polypropylene

EVA-ﬁlm

LLDPE

Average

54

78

328

372

SrA

2.5

8.4

83.6

30.4

SRB

6.4

14.1

120.3

111.1

rC

7.1

23.6

234.2

85.2

RD

17.9

39.4

336.9

311.1

ASr = within-laboratory standard deviation for the indicated material. It is

obtained by pooling the within-laboratory standard deviations of the test result from

all of the participating laboratories:

Sr = [[(S1)2 + (S2)2. . .+ (Sn)2]n]1/2

BSR = between-laboratories reproducibility, expressed as standard deviation:

SR = [Sr2 + SL2]1/2

where: SL is the standard deviation of laboratory means.

Cr = within-laboratory critical interval between two test results = 2.8 3 Sr.

DR = between laboratories critical interval between two test results = 2.8 3 SR.

15.1 Table 1 is based on a round robin conducted in 1989 in

accordance with Practice E 691, involving four materials tested

by nine laboratories. For each material, all the samples were

prepared at one source, but the individual specimens were

prepared at the laboratories which tested them. Each test result

was the average of ﬁve individual determinations. Each labo-

ratory obtained two test results for each material. (Warning—

The explanations of “r” and “R” (15.2 through 15.2.3) are only

Supporting data are available from ASTM Headquarters. Request RR: D20-

1024.

4

intended to present a meaningful way of considering the

approximate precision of this test method. The data presented

in Table 1 should not be applied to acceptance or rejection of

materials, as these data apply only to the materials tested in the

round robin and are unlikely to be rigorously representative of

other lots, formulations, conditions, materials, or laboratories.

Users of this test method should apply the principles outlined

in Practice E 691 to generate data speciﬁc to their materials and

laboratory (or between speciﬁc laboratories). The principles of

15.2 through 15.2.3 would then be valid for such data.)

15.2 Concept of “r” and “R” in Table 1—If Sr and SR have

been calculated from a large enough body of data, and for test

results that were averages from testing ﬁve specimens for each

test result, then:

15.2.1 Repeatability—“r” is the interval representing the

critical difference between two test results for the same

material, obtained by the same operator using the same

equipment on the same day in the same laboratory. Two test

results shall be judged not equivalent if they differ by more

than the “r” value for that material.

15.2.2 Reproducibility—“R” is the interval representing the

critical difference between two test results for the same

material, obtained by different operators using different equip-

ment in different laboratories, not necessarily on the same day.

Two test results shall be judged not equivalent if they differ by

more than the “R” value for that material.

15.2.3 Any judgement in accordance with 15.2.1 or 15.2.2

would have an approximate 95 % (0.95) probability of being

correct.

15.3 There are no recognized standards by which to esti-

mate bias of this test method.

16. Keywords

16.1 drop dart; impact; plastic ﬁlm

8

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 1709 – 04

APPENDIX

(Nonmandatory Information)

X1.

TABLE X1.1 Impact Values by Four Test Methods

MaterialA

D 3420 Procedure AB

J

PP, 1 mil

PP, 2 mil

LLDPE, 1 mil

LLDPE, 3.5 mil

A

B

D 3420 Procedure BC

J

0.27

0.65

0.41

0.97

g

D

D 1709

(Method A)

J

D

D 4272

ft · lb · f

F

J

0.09E

7.01E

0.49H

3.34H

0.30

0.95

0.52

1.43

75

47G

309I

C

0.49

0.30G

2.00I

0.07

5.17E

0.36H

2.46H

E

LLDPE (linear low density polyethylene).

Four laboratories, two sets of data each.

CEight laboratories, two sets of data each.

DMinimum weight of the tester was too heavy.

EOne laboratory, one set of data.

FThree laboratories, one set of data each.

GTwo laboratories, one set of data each.

HTwo laboratories, one set of data each.

IFive laboratories, one set of data each.

SUMMARY OF CHANGES

This section identiﬁes the location of selected changes to this test method. For the convenience of the user,

Committee D20 has highlighted those changes that may impact the use of this test method. This section may also

include descriptions of the changes or reasons for the changes, or both.

D 1709 – 04:

(1) Added footnote to Fig. 1.

D 1709 – 03:

(1) Added paragraph 5.3 and subsequent note.

(2) Added paragraph 14.1.4.

(3) Added paragraph 5.1.1 and subsequent two notes.

D 1709 – 01:

(1) Metric dimensions of the dart head were changed so they

are a direct conversion from the U.S. customary units.

D 1709 – 98:

(1) Last sentence of 5.3 was revised.

D 1709 – 97:

(1) Metric dimensional units were changed to hard metric to

harmonize with ISO 7765-1.

(2) Tolerances were added to the inch-pound dimensional

units in order to agree with the SI units.

(3) DiB was revised to meet current format requirements.

(4) In 9.9, a phrase was added to allow other symbols to be

used to designate failure and nonfailure.

ASTM International takes no position respecting the validity of any patent rights asserted in connection with any item mentioned

in this standard. Users of this standard are expressly advised that determination of the validity of any such patent rights, and the risk

of infringement of such rights, are entirely their own responsibility.

This standard is subject to revision at any time by the responsible technical committee and must be reviewed every ﬁve years and

if not revised, either reapproved or withdrawn. Your comments are invited either for revision of this standard or for additional standards

and should be addressed to ASTM International Headquarters. Your comments will receive careful consideration at a meeting of the

responsible technical committee, which you may attend. If you feel that your comments have not received a fair hearing you should

make your views known to the ASTM Committee on Standards, at the address shown below.

This standard is copyrighted by ASTM International, 100 Barr Harbor Drive, PO Box C700, West Conshohocken, PA 19428-2959,

United States. Individual reprints (single or multiple copies) of this standard may be obtained by contacting ASTM at the above

address or at 610-832-9585 (phone), 610-832-9555 (fax), or service@astm.org (e-mail); or through the ASTM website

(www.astm.org).

9

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758