BRITISH STANDARD

BS EN

1621-2:2003

Incorporating

Corrigendum No. 1

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Motorcyclists’

protective clothing

against mechanical

impact —

Part 2: Motorcyclists’ back protectors —

Requirements and test methods

The European Standard EN 1621-2:2003 has the status of a

British Standard

ICS 13.340.10

12 &23<,1* :,7+287 %6, 3(50,66,21 (;&(37 $6 3(50,77(' %< &23<5,*+7 /$:

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

BS EN 1621-2:2003

National foreword

This British Standard is the official English language version of

EN 1621-2:2003.

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

The UK participation in its preparation was entrusted by Technical Committee

PH/3, Protective clothing, to Subcommittee PH/3/9, Clothing for the protection

of riders of motorcycles, which has the responsibility to:

—

—

aid enquirers to understand the text;

present to the responsible international/European committee any

enquiries on the interpretation, or proposals for change, and keep the

UK interests informed;

monitor related international and European developments and

promulgate them in the UK.

—

A list of organizations represented on this subcommittee can be obtained on

request to its secretary.

WARNING The United Kingdom, as a member of CEN, is obliged to publish

EN 1621-2:2003 as a British Standard. However, attention is drawn to the fact that

during the development of this European Standard, the United Kingdom consistently

voted against its approval as a European Standard.

The reason for this disapproval is that during discussion of this standard by BSI

Committee PH/3/9, which mirrors the work of CEN Committee TC162, WG9, several

UK experts expressed the opinion that the transmitted force levels given as

requirements in this EN are too high.

BSI will assume no liability whatsoever for the failure on the part of any user of this

standard to consider this aspect.

Cross-references

The British Standards which implement international or European

publications referred to in this document may be found in the BSI Catalogue

under the section entitled “International Standards Correspondence Index”, or

by using the “Search” facility of the BSI Electronic Catalogue or of

British Standards Online.

This publication does not purport to include all the necessary provisions of a

contract. Users are responsible for its correct application.

Compliance with a British Standard does not of itself confer immunity

from legal obligations.

This British Standard, was

published under the authority

of the Standards Policy and

Strategy Committee on

3 September 2003

Summary of pages

This document comprises a front cover, an inside front cover, the EN title page,

pages 2 to 15 and a back cover.

The BSI copyright notice displayed in this document indicates when the

document was last issued.

Amendments issued since publication

Amd. No.

© BSI 24 February 2004

Date

Comments

15030

Corrigendum No. 1

24 February 2004 Correction to national foreword

ISBN 0 580 42566 5

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EUROPEAN STANDARD

NORME EUROPÉENNE

EUROPÄISCHE NORM

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

ICS 13.340.10

EN 1621-2

August 2003

English version

Motorcyclists' protective clothing against mechanical impact -

Part 2: Motorcyclists' back protectors - Requirements and test

methods

Vêtements de protection contre les chocs mécaniques pour

motocyclistes - Partie 2: Protecteurs dorsaux - Exigences

et méthodes d'essai

Motorradschutzkleidung gegen mechanische Belastung -

Teil 2: Rückenprotektoren - Anforderungen und

Prüfverfahren

This European Standard was approved by CEN on 2 July 2003.

CEN members are bound to comply with the CEN/CENELEC Internal Regulations which stipulate the conditions for giving this European

Standard the status of a national standard without any alteration. Up-to-date lists and bibliographical references concerning such national

standards may be obtained on application to the Management Centre or to any CEN member.

This European Standard exists in three official versions (English, French, German). A version in any other language made by translation

under the responsibility of a CEN member into its own language and notified to the Management Centre has the same status as the official

versions.

CEN members are the national standards bodies of Austria, Belgium, Czech Republic, Denmark, Finland, France, Germany, Greece,

Hungary, Iceland, Ireland, Italy, Luxembourg, Malta, Netherlands, Norway, Portugal, Slovakia, Spain, Sweden, Switzerland and United

Kingdom.

EUROPEAN COMMITTEE FOR STANDARDIZATION

COMITÉ EUROPÉEN DE NORMALISATION

EUROPÄISCHES KOMITEE FÜR NORMUNG

Management Centre: rue de Stassart, 36

B-1050 Brussels

© 2003 CEN

All rights of exploitation in any form and by any means reserved

worldwide for CEN national Members.

Ref. No. EN 1621-2:2003 E

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Contents

page

Foreword......................................................................................................................................................................3

Introduction .................................................................................................................................................................4

1

2

3

4

4.1

4.2

4.3

4.4

4.5

4.6

5

5.1

5.2

5.3

6

6.1

6.2

6.3

6.4

6.5

6.6

6.7

7

8

Scope ..............................................................................................................................................................5

Normative references ....................................................................................................................................5

Terms and definitions....................................................................................................................................5

Requirements .................................................................................................................................................6

General............................................................................................................................................................6

Innocuousness...............................................................................................................................................6

Minimum dimensions of zones of protection .............................................................................................7

Sizing and size marking ................................................................................................................................8

Ergonomic Requirements .............................................................................................................................8

Level of impact performance ........................................................................................................................8

Test Equipment - Apparatus .........................................................................................................................8

Dropping apparatus.......................................................................................................................................8

Bar impactor ...................................................................................................................................................8

Anvil ................................................................................................................................................................9

Test Method ..................................................................................................................................................10

Samples for technical examination and ergonomic testing....................................................................10

Preconditioning and testing atmosphere..................................................................................................10

Measurement and marking of back protectors.........................................................................................10

Procedures for impact testing ....................................................................................................................10

Number of tests............................................................................................................................................11

Test results ...................................................................................................................................................11

Test report ....................................................................................................................................................11

Marking .........................................................................................................................................................11

Information Supplied by the Manufacturer ...............................................................................................12

Annex A (normative) Ergonomic Tests ...................................................................................................................14

A.1General..........................................................................................................................................................14

A.2Tests..............................................................................................................................................................14

A.3Test report ....................................................................................................................................................14

Annex ZA (informative) Clauses of this European Standard addressing essential requirements or other

provisions of EU Directives ........................................................................................................................15

2

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Foreword

This document (EN 1621-2:2003) has been prepared by Technical Committee CEN /TC 162, "Protective clothing

including hand and arm protection and lifejackets", the secretariat of which is held by DIN.

This European Standard shall be given the status of a national standard, either by publication of an identical text or

by endorsement, at the latest by February 2004, and conflicting national standards shall be withdrawn at the latest

by February 2004.

This European Standard has been prepared under a mandate given to CEN by the European Commission and the

European Free Trade Association, and supports essential requirements of EU Directives.

For the relationship with EU Directives, see informative annex ZA, which is an integral part of this standard.

Annex A is normative.

This European Standard is one of a series of standards as listed below:

EN 1621-1 Motorcyclists’ protective clothing against mechanical impact — Part 1: Requirements and methods of

test for impact protectors

EN 13595-1 Protective clothing for professional motorcycle riders — Jackets, trousers and one-piece or divided

suits — Part 1: General requirements

EN 13595-2 Protective clothing for professional motorcycle riders — Jackets, trousers and one-piece or divided

suits — Part 2: Test method for determination of impact abrasion resistance

EN 13595-3 Protective clothing for professional motorcycle riders — Jackets, trousers and one-piece or divided

suits — Part 3: Test method for determination of burst strength

EN 13595-4 Protective clothing for professional motorcycle riders — Jackets, trousers and one-piece or divided

suits — Part 4: Test method for determination of impact cut resistance

According to the CEN/CENELEC Internal Regulations, the national standards organizations of the following

countries are bound to implement this European Standard: Austria, Belgium, Czech Republic, Denmark, Finland,

France, Germany, Greece, Hungary, Iceland, Ireland, Italy, Luxembourg, Malta, Netherlands, Norway, Portugal,

Slovakia, Spain, Sweden, Switzerland and the United Kingdom.

3

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Introduction

Motorcyclist’s back protectors are devices worn within or on top of other protective clothing, covering at least the

central part of the back from the waist to the neck. About 13% of motorcyclists injured in road accidents have an

injury to this back region. However, only 0,8% of the injured riders suffer a fracture of the spine and less than 0,2%

of injured riders have a serious back injury resulting in neurological damage. These serious injures are usually

caused by axial forces due to blows on the head, or bending and twisting forces on the back caused by blows to

the shoulders, hips and other parts of the body. Back protectors do not provide protection from these forces. The

majority of the more minor injuries are bruises and strains caused by direct blows, and back protectors can provide

some protection against these. The scapula is often injured (1,3%), protection should extend to cover this area.

The performance requirements have been chosen as a best practical compromise between protection, comfort,

and ergonomic requirements. Protectors that are too stiff or heavy will not be worn. The test methods are designed

to provide information on protection against impacts against edges such as kerb stones. The force levels in the

tests do not compare directly with the forces to which riders are exposed in accidents, but experiences have shown

that products meeting the requirements of this European Standard reduce the incidence and severity of injuries.

Motorcyclists' back protectors are sometimes combined with a product such as a body belt or lumbar support

designed to give support to the lower back in normal riding. These elements, within their limited size, can also

provide some impact protection, in this case they are to be called 'lumbar protectors' and are also covered by this

standard.

4

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

1

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Scope

This European Standard specifies the minimum coverage to be provided by motorcyclists’ back protectors worn by

riders in normal traffic situations. The standard contains the requirements for the performance of the protectors

under impact and details of the test methods. Requirements for sizing, ergonomic requirements, and requirements

for innocuousness, labelling and the provision of information are included.

The provision of this European Standard may not fully cover the needs of particular protectors (e.g. inflatable

protector or other types of protector).

2

Normative references

This European Standard incorporates by dated or undated reference, provisions from other publications. These

normative references are cited at the appropriate places in the text and the publications are listed below. In the

case of dated references, subsequent amendments to, or revisions of, any of these publications, apply to this

European Standard only when incorporated into it by amendment or revision. In the case of undated references the

latest edition of the publications referred to applies (including amendments).

EN 340, Protective clothing — General requirements.

EN 1621-1:1997, Motorcyclists' protective clothing against mechanical impact — Part 1: Requirements and test

methods for impact protectors.

ISO 6487, Road Vehicles — Measurement techniques in impact tests – Instrumentation.

ISO 7000, Graphical symbols for use on equipment — Index and synopsis.

3

Terms and definitions

For the purposes of this European Standard, the following terms and definitions apply:

3.1

general

3.1.1

motorcyclist's back protectors

motorcyclist’s back protectors are specific devices worn on the back that are intended to reduce the severity of

injuries caused by impacts

3.1.2

motorcyclist's lumbar protector

motorcyclist’s back protector with dimensions limited to cover the lumbar region; intended to reduce the severity of

injuries caused by impacts

3.1.3

zone of protection

the zone of protection is a specific area of the protective equipment that is intended to provide protection and this

area is subject to specific testing

NOTEThe minimum dimensions of the zones of protection will normally be marked on test specimens during the test

procedures.

5

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

3.2

body dimensions

the following body dimensions should be adequate for the designation of back protectors (see Figure 1)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

3.2.1

waist to shoulder

the maximum vertical length measured posteriorly from the waist to the junction of the shoulder to the neck

NOTE

This is an indication of torso length.

3.2.2

waist line

the maximum horizontal girth measured during normal breathing with the subject standing upright and the tape

measure passed around the body in the plane of the waist, 50mm above the supra-cristal plane which is at the

level of the highest points of the iliac crests

NOTEThe dimension of 50 mm refers to a subject of 1,78 m tall and should be scaled pro rata with the height of the actual

subject.

Key

1 – Waist to shoulder

2 – Waist line

Figure 1 — Body dimensions

4

Requirements

4.1 General

Motorcyclists’ back protectors shall meet an overall requirement that they are safe to use, comfortable to wear and

fit for their purpose.

4.2 Innocuousness

Construction materials and incorporated substances shall not endanger those coming into contact with them. The

manufacturer shall include in the information a declaration that to his knowledge no harmful substances are

contained in the product. The manufacturer shall give guidance on the safe destruction and disposal of the

products and of any hazards that could arise during mechanically disrupting or incinerating the product.

6

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

4.3 Minimum dimensions of zones of protection

Motorcyclists’ back protectors shall have a minimum zone of protection which shall be related to the size of the user

(see EN 340). The minimum dimensions of the zone of protection shall be determined from Tables 1 and 2.

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

b

a

Figure 2 – Minimum dimensions of zones of protection

Table 1 — Dimensions of minimum zone of protection for back protector

Dimensions in Figure 2a

A

72%

B

29%

C

44%

D

29%

All dimensions are referred to waist to shoulder length (100%) of the user

Table 2 — Dimensions of minimum zone of protection for lumbar protector

Dimensions in Figure 2b

E

32%

D

29%

All dimensions are referred to waist to shoulder length

(100%) of the user

7

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

The dimensions and position of the zone of protection, relative to the coverage provided by the whole product, shall

be given in the information supplied by the manufacturer (see 8).

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

4.4 Sizing and size marking

Motorcyclists’ back protectors shall be marked with their sizing using a pictogram according to EN 340. The I in a

book pictogram ISO 7000-1641 shall also be used. The pictograms are to be placed on the product and on the

package in which it is supplied.

4.5 Ergonomic Requirements

When examined and tested according to annex A, back protectors shall be found satisfactory for the use intended

and as indicated in the information supplied by the manufacturer.

4.6 Level of impact performance

Motorcyclists’ back protectors shall be impact tested with an impactor designed to represent the hazards of impacts

with edges such as kerbstones. The impactor shall be mounted on the appropriate guided falling mass. The

specified impact energy shall be within a limit deviation of 3%.

Level 1 protectors: The average peak force recorded below the anvil in the tests described in 6.4 shall be below

18kN, and no single value shall exceed 24kN.

Level 2 protectors: The average peak force recorded below the anvil in the tests described in 6.4 shall be below

9kN, and no single value shall exceed 12kN.

5

Test Equipment - Apparatus

5.1 Dropping apparatus

The apparatus shall be such that a mass (“falling weight”) can be released in order to drop along a guided vertical

path onto the sample placed on a test anvil. The centre of the mass of the falling weight shall lie over the centre of

the anvil.

5.2

Bar impactor

A bar impactor which shall be rectangular with a length, h1, equal to (160  2) mm, a width, h2, at the top, equal to

(50  1) mm and with a radius hemispherical face, R, equal to (12,5  0,1) mm shall be provided, see Figure 3. The

mass of the impactor and guided mass shall be (5 000  50) g and its kinetic energy on impact shall be (50  1.5) J.

8

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Figure 3 — Bar impactor

5.3

5.3.1

Anvil

General

The anvil shall be made of polished steel with the following dimensions l1 equal to (190  20) mm, l2 equal to

(100  2) mm and r1 equal to (150  5) mm, see Figure 4.

The anvil shall be attached through a piezoelectric load cell or equivalent force transducer to a mass of at least

1 000 kg. The load cell or force transducer shall be preloaded to the manufacturer’s instructions.

Key

1 load cell

Figure 4 — Anvil

NOTE

The anvil is designed to represent the back.

9

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

5.3.2

Force measurement instrumentation

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

The anvil shall be mounted so that during impact testing the whole force between the anvil and the massive base of

the apparatus passes through a quartz force transducer in line with it’s sensitive axis. The force transducer shall

have a calibrated range of not less that 50kN and a lower threshold of less than 0,5kN. The output of the force

transducer shall be processed by a charge amplifier and displayed and recorded on suitable instruments. The

recording system shall show a continuous force with a time record, or shall have a peak force detection capability.

Digital sampling systems shall have a minimum rate of 10kHz. The measuring system including the drop assembly

shall have a frequency response in accordance with channel frequency class (CFC) 1 000 of ISO 6487.

5.3.3

Tolerance and uncertainty

Measuring instruments or their independent working components unless otherwise specified shall have an error

limit of  2% of the pass/fail level of the characteristic being measured.

For each of the required sequences of measurements performed in accordance with this standard a corresponding

estimate of the uncertainty of the final result shall be determined. On request, this uncertainty (Um) shall be given in

the test report in the form Um =  X. It shall be used in determining whether a “Pass” performance has been

achieved. If the final result plus Um is above the maximum Pass level, the sample shall be deemed to have failed.

6

Test Method

6.1 Samples for technical examination and ergonomic testing

Back protectors shall be supplied by the manufacturer or his agent complete with labels, or copies of the proposed

labels, and the information supplied by the manufacturer that shall be supplied with the products. At least three

samples of back protectors shall be supplied for testing. If a manufacturer offers a size range one sample shall be

from the mid-point and one from the largest and smallest sizes.

6.2 Preconditioning and testing atmosphere

Back protectors shall be preconditioned and tested to the requirements as described in EN 1621-1:1997, subclause

6.1..

6.3 Measurement and marking of back/lumbar protectors

The required dimensions of the minimum zone of protection of the back/lumbar protector shall be determined from

their stated torso length, which shall correspond to Table 1 or Table 2, as applicable. Templates, see Figure 1, for

the minimum zone of protection shall be prepared from stiff but flexible material such as coated fabric or card. The

templates shall be accurately prepared (tolerances  5%). The templates shall be used to mark the perimeter of

the minimum zone of protection onto the outside of the back/lumbar protector with a felt tip pen or similar marker.

The correspondence between the lines marked on the back/lumbar protector by the template and the extent of the

protective structures shall be determined. Any apparent weak points, or points which appear to offer reduced

protection, shall also be marked.

6.4 Procedures for impact testing

Back protectors marked with the perimeter line of the minimum zone of protection and the examination marks

according to 6.3, and that have been pre-conditioned according to 6.2 shall be used.

Normally whole back protectors shall be tested. The sample shall be placed onto the centre of the anvil outside

surface upward. If it is necessary to reduce their size to fit within the test equipment the minimum zone of protection

may be cut into and partially removed for testing. Care should be taken to ensure that the cutting and removal of

parts of the back protector do not effect its performance during the impact tests. Cut edges shall be bound with

adhesive tape to retain the normal relationship between components of the protector.

10

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

6.5 Number of tests

A minimum of five impacts shall be carried out on each type of construction present using the equipment described

in clause 5. The impacts shall be distributed over the protectors. The centres of the impacts shall be more than

90mm apart. A series of at least five impacts shall be carried out, one shall be (40 ± 5) mm from the perimeter line

of the zone of protection, one shall be (60  5) mm from the perimeter line and one shall be at the centre of the

zone of protection. At least two single impacts shall also be made on all visually identified weak points and /or in

the direction found to be more severe.

The same test cycle shall be applied to other size if some contraction parameter is different (e.g. thickness).

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

6.6 Test results

Individual peak transmitted forces shall be reported and the average peak force shall be calculated and reported

6.7 Test report

The test report shall include the following information:

a) identification of the back protector, including source and date of receipt;

b) the method used by reference to this European Standard;

c) results of the test;

d) if relevant, any deviations from the method specified in this European Standard;

e) any unusual features observed during the test;

f)

date of test;

g) identification of the laboratory carrying out the test.

7

Marking

Motorcyclists back protectors shall be permanently and conspicuously marked with at least the following:

a)

b)

the number of the specific European Standard, (EN 1621-2);

The name or trade mark of the manufacturer or his authorised representative in the European Union or country

where the product is placed on the market;

identification of the product type, commercial name or code;

the size designation of the item, (waist to shoulder length as described in 4.4);

a pictogram showing the performance level and a type of protector, “B” for back protector, or “L” for lumbar

protector (a suitable Pictogram is shown in Figure 5).

c)

d)

e)

11

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

B

2

EN 1621-2

Figure 5 — Pictogram

8

Information Supplied by the Manufacturer

Motorcyclists back/lumbar protectors shall be supplied with information and instructions for fitting and use. These

are an essential part of protective equipment. They shall contain at least the following information in the official

language(s) of the state or region in which they are placed on the market. The following information should be

given on the product whenever practical.

1) The name and address of the manufacturer or his authorised representative;

2) the type of use for which the protectors are intended including any relevant restrictions;

3) the hazards specific to motorcycling against which some protection is given;

4) the hazards specific to motorcycling against which protection is NOT given;

5) international care label symbols(Negative labels are important);

6) all the information required in section 7: Marking;

7) how to adjust the back/lumbar protector;

8) performance recorded during technical tests;

9) a warning about any changes in environmental conditions, such as temperature, that would significantly reduce

the performance of the back/lumbar protector;

10) the dimensions of the Zone of protection , relative to the coverage provided by the whole product;

11) a warning that no back/lumbar protector can offer full protection against injury;

12) a specific warning that spinal injuries will not be prevented by the back/lumbar protector;

13) a warning about any contamination, alteration to the back/lumbar protector, or misuse that would dangerously

reduce the performance of the back/lumbar protector;

14) a declaration that no harmful substances are contained in the product;

12

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

15) instructions for caring for and cleaning the back/lumbar protector;

16) instructions concerning inspection and repair of the back/lumbar protector, when to replace it and how to

decide if it no longer provides adequate protection;

17) instructions for the safe destruction and disposal of the back/lumbar protectors and of any hazards that could

arise during mechanically disrupting or incinerating the product.

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

13

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Annex A

(normative)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Ergonomic Tests

A.1 General

The back protector is examined visually to assess torsional and bending flexibility to ensure no restriction in

movement. The back protector should also be examined visually for design features that may cause problems and

any sharp edges.

The back protector is then put on by an assessor of suitable size and with experience of riding a motorcycle who

then carries out the following tests.

A.2 Tests

1)

2)

3)

4)

5)

6)

can you get on and off a Motorcycle;

can you comfortably reach the controls of the Motorcycle;

can you turn your head and torso when on a Motorcycle;

does the adjustment system cause discomfort;

does the adjustment system securely hold the protector in place;

can you pick something up from the floor by bending forward.

A.3 Test report

The test report shall include the following:

1)

2)

3)

4)

5)

Reference to this test method of this annex;

description of the test protector;

name, sex and dimensions of the assessor,(Waist to Shoulder length);

any deviations from the specified procedure;

specific reasons for failure of any of the ergonomic tests.

14

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN 1621-2:2003 (E)

Annex ZA

(informative)

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Clauses of this European Standard addressing essential requirements or

other provisions of EU Directives

This European Standard has been prepared under a mandate given to CEN by the European Commission and the

European Free Trade Association and supports essential requirements of Directive 89/686/EEC.

WARNING : Other requirements and other EU Directives may be applicable to the product(s) falling within the

scope of this standard.

The following clauses of this standard are likely to support requirements of Directive 89/686/EEC, Annex II.

Table ZA.1 — Relationship between this European Standard and Directive 89/686/EEC

Clauses of this European Standard

Directive 89/686/EEC, Annex II

1 General requirements applicable to PPE

1.1

4.5 and annex A

1.1.1

1.1.2

annex A

4.3; 4.6

Design Principles

Ergonomics

Levels and classes of protection

1.1.2.1 Highest level of protection possible

1.1.2.2 Classes of protection appropriate to different levels of risk

1.2

Innocuousness

4.2

annex A

1.2.1.1 Suitable constituent materials

1.2.1.3 Maximum permissible user impediment

1.3

4.3 – 6.3

8

4.5 and annex A

4.4 and 7

4.6 - 6.4

1.3.1

1.4

2.1

Comfort and efficiency

Adaption to user morphology

Information supplied by the manufacturer

PPE incorporating adjustment systems

2.12PPE bearing one or more identification or recognition marks

directlyor indirectly relating to health and safety

3.1 .1

Impact caused by falling or projecting objects and collision of parts of the

body with obstacles

Compliance with the clauses of this European Standard provides one means of conforming with the specific

essential requirements of the Directive concerned and associated EFTA regulations.

15

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

BS EN

1621-2:2003

BSI — British Standards Institution

BSI is the independent national body responsible for preparing

British Standards. It presents the UK view on standards in Europe and at the

international level. It is incorporated by Royal Charter.

Licensed Copy: sheffieldun sheffieldun, na, Fri Nov 17 08:07:13 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Revisions

British Standards are updated by amendment or revision. Users of

British Standards should make sure that they possess the latest amendments or

editions.

It is the constant aim of BSI to improve the quality of our products and services.

We would be grateful if anyone finding an inaccuracy or ambiguity while using

this British Standard would inform the Secretary of the technical committee

responsible, the identity of which can be found on the inside front cover.

Tel: +44 (0)20 8996 9000. Fax: +44 (0)20 8996 7400.

BSI offers members an individual updating service called PLUS which ensures

that subscribers automatically receive the latest editions of standards.

Buying standards

Orders for all BSI, international and foreign standards publications should be

addressed to Customer Services. Tel: +44 (0)20 8996 9001.

Fax: +44 (0)20 8996 7001. Email: orders@bsi-global.com. Standards are also

available from the BSI website at http://www.bsi-global.com.

In response to orders for international standards, it is BSI policy to supply the

BSI implementation of those that have been published as British Standards,

unless otherwise requested.

Information on standards

BSI provides a wide range of information on national, European and

international standards through its Library and its Technical Help to Exporters

Service. Various BSI electronic information services are also available which give

details on all its products and services. Contact the Information Centre.

Tel: +44 (0)20 8996 7111. Fax: +44 (0)20 8996 7048. Email: info@bsi-global.com.

Subscribing members of BSI are kept up to date with standards developments

and receive substantial discounts on the purchase price of standards. For details

of these and other benefits contact Membership Administration.

Tel: +44 (0)20 8996 7002. Fax: +44 (0)20 8996 7001.

Email: membership@bsi-global.com.

Information regarding online access to British Standards via British Standards

Online can be found at http://www.bsi-global.com/bsonline.

Further information about BSI is available on the BSI website at

http://www.bsi-global.com.

Copyright

Copyright subsists in all BSI publications. BSI also holds the copyright, in the

UK, of the publications of the international standardization bodies. Except as

permitted under the Copyright, Designs and Patents Act 1988 no extract may be

reproduced, stored in a retrieval system or transmitted in any form or by any

means – electronic, photocopying, recording or otherwise – without prior written

permission from BSI.

This does not preclude the free use, in the course of implementing the standard,

of necessary details such as symbols, and size, type or grade designations. If these

details are to be used for any other purpose than implementation then the prior

written permission of BSI must be obtained.

Details and advice can be obtained from the Copyright & Licensing Manager.

Tel: +44 (0)20 8996 7070. Fax: +44 (0)20 8996 7553.

Email: copyright@bsi-global.com.

BSI

389 Chiswick High Road

London

W4 4AL

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758