BRITISH STANDARD

BS EN ISO

2039-1:2003

Incorporating

Corrigendum No. 1

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Plastics —

Determination of

hardness —

Part 1: Ball indentation method

The European Standard EN ISO 2039-1:2003 has the status of a

British Standard

ICS 83.080.01

12 &23<,1* :,7+287 %6, 3(50,66,21 (;&(37 $6 3(50,77(' %< &23<5,*+7 /$:

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

BS EN ISO 2039-1:2003

National foreword

This British Standard is the official English language version of

EN ISO 2039-1:2003. It is identical with ISO 2039-1:2001. It supersedes

BS EN ISO 2039-1:1997 which is withdrawn.

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

The UK participation in its preparation was entrusted to Technical Committee

PRI/21, Plastic test methods, which has the responsibility to:

—

—

aid enquirers to understand the text;

present to the responsible international/European committee any

enquiries on the interpretation, or proposals for change, and keep the

UK interests informed;

monitor related international and European developments and

promulgate them in the UK.

—

A list of organizations represented on this committee can be obtained on

request to its secretary.

Cross-references

The British Standards which implement international or European

publications referred to in this document may be found in the BSI Catalogue

under the section entitled “International Standards Correspondence Index”, or

by using the “Search” facility of the BSI Electronic Catalogue or of

British Standards Online.

This publication does not purport to include all the necessary provisions of a

contract. Users are responsible for its correct application.

Compliance with a British Standard does not of itself confer immunity

from legal obligations.

This British Standard was

published under the authority

of the Standards Policy and

Strategy Committee on

27 February 2003

Summary of pages

This document comprises a front cover, an inside front cover, the EN ISO title

page, the EN ISO foreword page, the ISO title page, pages ii to iv, pages 1 to 6,

the Annex ZA page and a back cover.

The BSI copyright date displayed in this document indicates when the

document was last issued.

Amendments issued since publication

Amd. No.

14433

© BSI 3 April 2003

Corrigendum No. 1

Date

3 April 2003

Comments

Corrected EN ISO foreword page

ISBN 0 580 41325 X

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EUROPEAN STANDARD

NORME EUROPÉENNE

EUROPÄISCHE NORM

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

ICS 83.080.01

EN ISO 2039-1

February 2003

Supersedes EN ISO 2039-1:1996

English version

Plastics - Determination of hardness - Part 1: Ball indentation

method (ISO 2039-1:2001)

Plastiques - Détermination de la dureté - Partie 1: Méthode

de pénétration à la bille (ISO 2039-1:2001)

Kunststoffe - Bestimmung der Härte - Teil 1:

Kugeleindruckversuch (ISO 2039-1:2001)

This European Standard was approved by CEN on 12 December 2002.

CEN members are bound to comply with the CEN/CENELEC Internal Regulations which stipulate the conditions for giving this European

Standard the status of a national standard without any alteration. Up-to-date lists and bibliographical references concerning such national

standards may be obtained on application to the Management Centre or to any CEN member.

This European Standard exists in three official versions (English, French, German). A version in any other language made by translation

under the responsibility of a CEN member into its own language and notified to the Management Centre has the same status as the official

versions.

CEN members are the national standards bodies of Austria, Belgium, Czech Republic, Denmark, Finland, France, Germany, Greece,

Hungary, Iceland, Ireland, Italy, Luxembourg, Malta, Netherlands, Norway, Portugal, Slovak Republic, Spain, Sweden, Switzerland and

United Kingdom.

EUROPEAN COMMITTEE FOR STANDARDIZATION

COMITÉ EUROPÉEN DE NORMALISATION

EUROPÄISCHES KOMITEE FÜR NORMUNG

Management Centre: rue de Stassart, 36

B-1050 Brussels

© 2003 CEN

All rights of exploitation in any form and by any means reserved

worldwide for CEN national Members.

Ref. No. EN ISO 2039-1:2003 E

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

CORRECTED 2003-02-05

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Foreword

The text of ISO 2039-1:2001 has been prepared by Technical Committee ISO/TC 61 "Plastics"

of the International Organization for Standardization (ISO) and has been taken over as EN ISO

2039-1:2003 by Technical Committee CEN/TC 249 "Plastics", the secretariat of which is held by

IBN.

This European Standard shall be given the status of a national standard, either by publication of

an identical text or by endorsement, at the latest by August 2003, and conflicting national

standards shall be withdrawn at the latest by August 2003.

This document supersedes EN ISO 2039-1:1996.

According to the CEN/CENELEC Internal Regulations, the national standards organizations of

the following countries are bound to implement this European Standard: Austria, Belgium, Czech

Republic, Denmark, Finland, France, Germany, Greece, Hungary, Iceland, Ireland, Italy,

Luxembourg, Malta, Netherlands, Norway, Portugal, Slovakia, Spain, Sweden, Switzerland and

the United Kingdom.

Endorsement notice

The text of ISO 2039-1:2001 has been approved by CEN as EN ISO 2039-1:2003 without any

modifications.

NOTE Normative references to International Standards are listed in Annex ZA (normative).

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

INTERNATIONAL

STANDARD

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

ISO

2039-1

Third edition

2001-12-01

Plastics — Determination of hardness —

Part 1:

Ball indentation method

Plastiques — Détermination de la dureté —

Partie 1: Méthode de pénétration à la bille

Reference number

ISO 2039-1:2001(E)

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

lcsid FDParemi

ihTs PDF file mc yatnoaie nmt deddebyfepca.se Icca ncnadrow eitA h'ebods licsneilop gnic,y tihs file mirp eb yatniv ro deewb detu slahl ton

ide ebtlnu desse tt ehyfepacse wihce era hml era deddebicsnede to i dnasntlalde t noeh comtupfrep remroign tide ehti.gn Iwod nnlidaogn tihs

fil,e trapies ccatpe tiereht nsnopser ehiiblity fo ton ifnriignA gn'ebods licnesilop gnic.y I ehTStneC Oarl Scerteiraat cacpets l oniibality it nihs

.aera

Ai ebods a tedarmfo kra Aebod SystemI snctaropro.de

teDials fo ts ehfotworp eracudts ust dec ortaet eihs PDF filc eeb na fi dnuot nlareneG eh Ifnler otait evt of ehil;e tP ehD-Fcrtaeiarap nomtesre

wretpo eimizf deirp rotni.gn Evyre csah era t neebkat nesne ot eruaht tf ehili es siutlbaf esu roI yb eSO memidob rebse. It neh lnuikletneve y

ttah a lborpem leratign ti ot is fnuo,d lpsaee ifnrom ttneC ehlar Secrteirata at tsserdda eh igleb nevwo.

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

© ISO 1002

Athgir lls serevr.de selnUs towrehise specfi,dei trap on fo this ilbupctanoi may cudorper ebtu ro deziliyna ni de fomr yb ro nam y,snae lecetinorc

m roecinahcal, inclidutohp gnocpoiym dna gnicrfoilm, wittuoh repmissii now nritif gnrom ietreh ISa Ot tserdda ehs lebwo I roS'Os membre ydob

it neh ctnuoo yrf ttseuqer eh.re

ISO cirypothg fofice

saCe tsopale 65 1121-HC 02 av

leT. 4 + 10 947 22 1 11

xaF0 947 22 14 + 9 74

E-mial coirypthgi@s.oc h

Web ww.wiso.ch

Prnietdi nS wztierland

ii

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Contents

Page

Foreword.....................................................................................................................................................................iv

1

2

3

4

5

6

7

8

9

10

Scope .............................................................................................................................................................. 1

Normative reference ...................................................................................................................................... 1

Term and definition ....................................................................................................................................... 1

Principle.......................................................................................................................................................... 1

Apparatus ....................................................................................................................................................... 2

Test specimens.............................................................................................................................................. 2

Conditioning................................................................................................................................................... 2

Procedure ....................................................................................................................................................... 2

Expression of results .................................................................................................................................... 3

Test report ...................................................................................................................................................... 4

Annex A (informative) Value of the ball indentation hardness as a function of the depth of penetration

and the test load ............................................................................................................................................ 5

iii

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Foreword

ISO (the International Organization for Standardization) is a worldwide federation of national standards bodies (ISO

member bodies). The work of preparing International Standards is normally carried out through ISO technical

committees. Each member body interested in a subject for which a technical committee has been established has

the right to be represented on that committee. International organizations, governmental and non-governmental, in

liaison with ISO, also take part in the work. ISO collaborates closely with the International Electrotechnical

Commission (IEC) on all matters of electrotechnical standardization.

International Standards are drafted in accordance with the rules given in the ISO/IEC Directives, Part 3.

The main task of technical committees is to prepare International Standards. Draft International Standards adopted

by the technical committees are circulated to the member bodies for voting. Publication as an International

Standard requires approval by at least 75 % of the member bodies casting a vote.

Attention is drawn to the possibility that some of the elements of this part of ISO 2039 may be the subject of patent

rights. ISO shall not be held responsible for identifying any or all such patent rights.

ISO 2039-1 was prepared by Technical Committee ISO/TC 61, Plastics, Subcommittee SC 2, Mechanical

properties.

This third edition cancels and replaces the second edition (ISO 2039-1:1993), subclause 8.3 and annex A of which

have been technically revised.

ISO 2039 consists of the following parts, under the general title Plastics — Determination of hardness:





Part 1: Ball indentation method

Part 2: Rockwell hardness

Annex A of this part of ISO 2039 is for information only.

iv

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

INTENRATIONAL TSANDADR

IS-9302 O1:(1002)E

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Plastics — Determination of hardness —

Part 1:

Ball indentation method

1

Scope

This part of ISO 2039 specifies a method for determining the hardness of plastics and ebonite by means of a

loaded ball indenter.

The ball indentation hardness determined by this method may provide data for research and development, quality

control and acceptance or rejection under specifications.

2

Normative reference

The following normative document contains provisions which, through reference in this text, constitute provisions of

this part of ISO 2039. For dated references, subsequent amendments to, or revisions of, any of these publications

do not apply. However, parties to agreements based on this part of ISO 2039 are encouraged to investigate the

possibility of applying the most recent edition of the normative document indicated below. For undated references,

the latest edition of the normative document referred to applies. Members of ISO and IEC maintain registers of

currently valid International Standards.

ISO 291:1997, Plastics — Standard atmospheres for conditioning and testing

3

Term and definition

For the purposes of this part of ISO 2039, the following term and definition apply.

3.1

ball indentation hardness

HB

the quotient of the load on the ball indenter by the surface area of the impression caused by the ball indenter after

a specified time of load application

NOTE

It is expressed in newtons per square millimetre.

4

Principle

The method consists of forcing a ball under a specified load into the surface of the test specimen. The depth of

impression is measured under load. The surface area of the impression is computed from its depth. The ball

indentation hardness is then calculated from the following relationship:

Ball indentation hardness = Applied load/Surface area of impression

1

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

5

Apparatus

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

5.1 Hardness tester, consisting essentially of a frame with an adjustable platform fitted with a plate to support

the test specimen, an indenter with its associated fittings and a device for applying the load without impact.

The tester shall also be equipped with a device to measure the depth of penetration of the indenter over a range of

0,4 mm with an accuracy of 0,005 mm.

The frame shall not be deformed under the maximum load by more than 0,05 mm, the deformation being measured

along the main axis of the applied force.

The indenter shall be a hardened and polished steel ball. The ball shall not show any deformation or damage after

the test.

The diameter of the ball shall be (5,0 0,05) mm.

5.2

Timing device, accurate to 0,1 s

6

Test specimens

Each test specimen shall be a smooth flat sheet or block of sufficient size to minimize edge effects on the test

result; for example 20 mm ¥ 20 mm. The surfaces of the test specimen shall be parallel. A thickness of 4 mm is

recommended.

The supported surface of the test specimen shall not show any deformation after testing.

NOTE 1If test specimens with thicknesses less than 4 mm are to be tested, it is possible to stack several test specimens on

top of each other. However, hardness values obtained on stacked test specimens and on single test specimens of the same

thickness may be different.

NOTE 2Although every effort should be made to ensure the parallelism of the specimen, there are some cases, especially

specimens injection-moulded from semi-crystalline thermoplastics, where it is difficult to obtain test specimens that are exactly

flat. If such slightly warped test specimens are used, part of the measured “depth of impression” will in fact correspond to the

distance travelled by the indenter in pressing the test specimen down on to the supporting plate. This difficulty can be overcome

by using a circular supporting plate of diameter (10 1) mm. This diameter is also sufficiently large for perfectly flat test

specimens. Also recommended is that the test specimen be placed with the flatter side towards the support plate.

7

Conditioning

Condition the test specimens, prior to testing, in one of the standard atmospheres specified in ISO 291.

8

8.1

Procedure

Unless otherwise specified, carry out the tests in the same atmosphere as was used for conditioning.

8.2 Place the test specimen on the supporting plate so that the test specimen is fully supported and its surfaces

are perpendicular to the direction of the applied load.

Apply an initial load F0 of (9,8 0,1) N at a point not less than 10 mm from the edge of the test specimen. Set the

depth-indicating device to zero and then smoothly apply the test load Fm (see 8.3) over a period of 2 to 3 s.

2

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

8.3

Choose the test load Fm from the values

49,0 N;

132 N;

358 N;

961 N

(tolerance 1 %)

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

such that the depth of impression h after correction for deformation of the frame (see 8.7) is between 0,15 mm and

0,35 mm.

If values of the depth of impression after 30 s are outside this range (either in the case of a series of test specimens

or in the case of an individual test specimen), change the test load to obtain a depth of impression within the range

specified above. The number of test measurements which do not give correct depths of impression shall be

reported.

If in a series of tests the test load has to be changed, the difference of hardness values occurring in the transition

region between different test loads may lead to difficulties in the interpretation of the test results, e.g. when

assessing the influence of heat ageing on hardness. In such cases, it is acceptable, by agreement between the

interested parties, to extend the range of depths of impression beyond the limits given above, but not by more than

20 % of the range. Use that test load for which the majority of depths of impression of the test series in question lie

between 0,15 mm and 0,35 mm.

8.4 Carry out the test in such a manner that any bubbles or cracks in the test specimen do not influence the

results. If several determinations are carried out on the same test specimen, ensure that the points of application of

the indenter are not less than 10 mm apart from each other and from the edge of the test specimen.

8.5 After 30 s of application of the test load Fm, measure the depth of impression under load, h1, with the

accuracy specified in 5.1.

8.6

Make ten valid tests on one or more test specimens.

8.7 Determine the deformation of the frame of the apparatus, h2, in millimetres, as follows: Place a soft copper

block (at least 6 mm thick) on the supporting plate and apply the initial load F0. Set the depth-indicating device to

zero and apply the test load Fm. Maintain the test load until the depth indicator is stationary. Note the reading,

remove the test load and reset the depth indicator to zero.

Repeat this sequence of operations until the reading of the depth indicator is constant after each application of the

test load. This represents the point at which no further penetration of the copper block takes place and therefore

the constant depth reading is the movement of the depth-indicating device due to the deformation of the frame of

the apparatus. Note this constant reading as h2. The corrected depth of impression h is given by h = h1 −h2.

9

9.1

Expression of results

Calculate the reduced test load Fr, in newtons, as follows:

Fr = Fm ¥

where

Fm

hr

h1

a

( h - hr ) + a

= Fm ¥

0,21

h - 0,25 + 0,21

is the load, in newtons, on the indenter;

is the reduced depth of impression (= 0,25 mm);

is the depth of impression, in millimetres, under the test load on the indenter;

3

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

h2

h

is the deformation, in millimetres of the test apparatus under the test load;

(= h1 – h2) is the depth of impression, in millimetres, after correcting for the deformation of the frame;

0,21) is a constant.

The values of hr and a are taken from a paper by H.H. Racké and Th. Fett in Materialprüfung, 10 (1968), No. 7,

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

a

NOTE

p. 226.

9.2

Calculate the ball indentation hardness from the equation

HB =

where

HB

Fr

hr

d

9.3

Fr

p d hr

is the ball indentation hardness, in newtons per square millimetre;

is the reduced test load, in newtons (see 9.1);

is the reduced depth of impression, in millimetres (= 0,25 mm);

is the diameter of the ball indenter (= 5 mm).

For values of HB lower than 250 N/mm2, round to the nearest 1 N/mm2.

For values of HB greater than 250 N/mm2, round to the nearest multiple of 10 N/mm2.

10 Test report

The test report shall include the following particulars:

a)

b)

c)

d)

e)

f)

g)

h)

a reference to this part of ISO 2039;

all details necessary for complete identification of the material tested;

the conditioning and the conditions under which the tests were carried out;

a description, the dimensions and the manner of preparation of the test specimens;

the number of tests averaged;

the number of tests which resulted in incorrect depths of impression;

the ball indentation hardness, average value and standard deviation;

the date of testing.

4

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

Annex A

(informative)

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Value of the ball indentation hardness as a function of the depth of

penetration and the test load

The values of HB in Table A.1 were calculated using the equations given in 9.1 and 9.2. When the corrected depth

of impression h has been determined (see 8.7), the table can thus be used to read the value of HB directly.

Table A.1

Depth of

impression, h

mm

0,150

0,155

0,160

0,165

0,170

0,175

0,180

0,185

0,190

0,195

0,200

0,205

0,210

0,215

0,220

0,225

0,230

0,235

0,240

0,245

0,250

0,255

0,260

0,265

0,270

0,275

0,280

0,285

0,290

0,295

0,300

0,305

0,310

0,315

0,320

0,325

0,330

0,335

0,340

0,345

0,350

49 N

23,82

22,79

21,84

20,96

20,16

19,41

18,72

18,07

17,47

16,91

16,38

15,88

15,41

14,97

14,56

14,16

13,79

13,44

13,10

12,78

12,48

12,19

11,91

11,65

11,39

11,15

10,92

10,70

10,48

10,28

10,08

9,89

9,70

9,53

9,36

9,19

9,04

8,88

8,73

8,59

8,45

Ball indentation hardness HB

in N/mm2 for test loads Fm of

132 N

64,17

61,38

58,82

56,47

54,30

52,29

50,42

48,68

47,06

45,54

44,12

42,78

41,52

40,34

39,22

38,16

37,15

36,20

35,29

34,43

33,61

32,83

32,09

31,37

30,69

30,04

29,41

28,81

28,24

27,68

27,15

26,64

26,14

25,67

25,21

24,77

24,34

23,93

23,53

23,14

22,77

358 N

174,04

166,47

159,54

153,16

147,26

141,81

136,75

132,03

127,63

123,51

119,65

116,03

112,61

109,40

106,36

103,48

100,76

98,18

95,72

93,39

91,16

89,04

87,02

85,09

83,24

81,47

79,77

78,14

76,58

75,08

73,63

72,24

70,91

69,62

68,37

67,17

66,02

64,90

63,81

62,77

61,76

961 N

467,19

446,87

428,25

411,12

395,31

380,67

367,07

354,42

342,60

331,55

321,19

311,46

302,30

293,66

285,50

277,79

270,48

263,54

256,95

250,69

244,72

239,03

233,59

228,40

223,44

218,68

214,13

209,76

205,56

201,53

197,66

193,93

190,34

186,87

183,54

180,32

177,21

174,21

171,30

168,49

165,78

5

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

NOTEWhen the ball indentation hardness of a test specimen is in the transition zone between one test load and the next,

slight differences in the ball indentation hardness may result if the test is carried out either with the smaller test load at a low

depth of penetration or with the larger test load at a high depth of penetration. In such cases, it is recommended that the test

load to be used be agreed upon between the interested parties.

6

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

EN ISO 2039−1:2003

Annex ZA

(normative)

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Normative references to international publications

with their relevant European publications

This European Standard incorporates by dated or undated reference, provisions from other

publications. These normative references are cited at the appropriate places in the text and the

publications are listed hereafter. For dated references, subsequent amendments to or revisions of

any of these publications apply to this European Standard only when incorporated in it by

amendment or revision. For undated references the latest edition of the publication referred to

applies (including amendments).

NOTE Where an International Publication has been modified by common modifications, indicated

by (mod.), the relevant EN/HD applies.

Publication

ISO 291

Year

1997

Title

Plastics - Standard

conditioning and testing

atmospheres

for

EN

EN ISO 291

Year

1997

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

BS EN ISO

2039-1:2003

BSI — British Standards Institution

BSI is the independent national body responsible for preparing

British Standards. It presents the UK view on standards in Europe and at the

international level. It is incorporated by Royal Charter.

Licensed Copy: sheffieldun sheffieldun, na, Mon Nov 20 02:44:59 GMT+00:00 2006, Uncontrolled Copy, (c) BSI

Revisions

British Standards are updated by amendment or revision. Users of

British Standards should make sure that they possess the latest amendments or

editions.

It is the constant aim of BSI to improve the quality of our products and services.

We would be grateful if anyone finding an inaccuracy or ambiguity while using

this British Standard would inform the Secretary of the technical committee

responsible, the identity of which can be found on the inside front cover.

Tel: +44 (0)20 8996 9000. Fax: +44 (0)20 8996 7400.

BSI offers members an individual updating service called PLUS which ensures

that subscribers automatically receive the latest editions of standards.

Buying standards

Orders for all BSI, international and foreign standards publications should be

addressed to Customer Services. Tel: +44 (0)20 8996 9001.

Fax: +44 (0)20 8996 7001. Email: orders@bsi-global.com. Standards are also

available from the BSI website at http://www.bsi-global.com.

In response to orders for international standards, it is BSI policy to supply the

BSI implementation of those that have been published as British Standards,

unless otherwise requested.

Information on standards

BSI provides a wide range of information on national, European and

international standards through its Library and its Technical Help to Exporters

Service. Various BSI electronic information services are also available which give

details on all its products and services. Contact the Information Centre.

Tel: +44 (0)20 8996 7111. Fax: +44 (0)20 8996 7048. Email: info@bsi-global.com.

Subscribing members of BSI are kept up to date with standards developments

and receive substantial discounts on the purchase price of standards. For details

of these and other benefits contact Membership Administration.

Tel: +44 (0)20 8996 7002. Fax: +44 (0)20 8996 7001.

Email: membership@bsi-global.com.

Information regarding online access to British Standards via British Standards

Online can be found at http://www.bsi-global.com/bsonline.

Further information about BSI is available on the BSI website at

http://www.bsi-global.com.

Copyright

Copyright subsists in all BSI publications. BSI also holds the copyright, in the

UK, of the publications of the international standardization bodies. Except as

permitted under the Copyright, Designs and Patents Act 1988 no extract may be

reproduced, stored in a retrieval system or transmitted in any form or by any

means – electronic, photocopying, recording or otherwise – without prior written

permission from BSI.

This does not preclude the free use, in the course of implementing the standard,

of necessary details such as symbols, and size, type or grade designations. If these

details are to be used for any other purpose than implementation then the prior

written permission of BSI must be obtained.

Details and advice can be obtained from the Copyright & Licensing Manager.

Tel: +44 (0)20 8996 7070. Fax: +44 (0)20 8996 7553.

Email: copyright@bsi-global.com.

BSI

389 Chiswick High Road

London

W4 4AL

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758