Designation: D 3574 – 05

Standard Test Methods for

Flexible Cellular Materials—Slab, Bonded, and Molded

Urethane Foams1

This standard is issued under the ﬁxed designation D 3574; the number immediately following the designation indicates the year of

original adoption or, in the case of revision, the year of last revision. A number in parentheses indicates the year of last reapproval. A

superscript epsilon (e) indicates an editorial change since the last revision or reapproval.

This standard has been approved for use by agencies of the Department of Defense.

1. Scope*

1.1 These test methods apply to slab, bonded, and molded

ﬂexible cellular products known as urethane foams. Urethane

foam may be generally deﬁned as an expanded cellular product

produced by the interaction of active hydrogen compounds,

water, and isocyanates.

1.2 This standard does not purport to address all of the

safety concerns, if any, associated with its use. It is the

responsibility of the user of this standard to establish appro-

priate safety and health practices and determine the applica-

bility of regulatory limitations prior to use.

1.3 The values stated in SI units are to be regarded as

standard.

NOTE 1—There is no equivalent ISO standard, however certain test

methods in this standard have similar or equivalent ISO standards and are

listed in the scope of the individual test method sections.

E 691 Practice for Conducting an Interlaboratory Study to

Determine the Precision of a Test Method

3. Terminology

3.1 Deﬁnitions of Terms Speciﬁc to This Standard:

3.1.1 bonded foam—a product produced by the adhesion of

small pieces of urethane foam to each other with a suitable

bonding agent.

3.1.2 core—the internal portion of a molded part, free of

skin.

3.1.3 cored foam—a ﬂexible cellular material containing a

multiplicity of holes (usually, but not necessarily, cylindrical in

shape), molded or cut into the material in some pattern,

normally perpendicular to the foam rise direction, and extend-

ing part or all the way through the piece

3.1.4 convoluted foam—a ﬂexible cellular material spe-

cially cut into sheets with “egg carton”-like dimples. The

dimple peaks and bases can have varied shapes and dimen-

sions.

3.1.5 ﬂexible cellular product—a cellular organic polymeric

material that will not rupture when a specimen 200 by 25 by 25

mm is bent around a 25-mm diameter mandrel at a uniform rate

of one lap in 5 s at a temperature between 18 and 29°C.

3.1.6 molded foam—a cellular product having the shape of

the enclosed chamber in which it is produced by foaming.

3.1.7 skin—the smooth surface layer of a molded foam

product, formed by contact with the mold or surfaces.

3.1.8 slab—a section of foam that is cut from the internal

portion of a large bun.

3.1.9 urethane foam—a ﬂexible cellular product produced

by the interaction of active hydrogen compounds, water, and

isocyanates.

3.1.10 viscoelastic foam—a specially formulated urethane

foam characterized by having slow recovery, low resilience,

and high hysteresis loss.

4. Summary of Test Methods

4.1 Unless speciﬁcally stated otherwise between the sup-

plier and the purchaser, all tests shall be made in accordance

with the methods speciﬁed in Sections 9-124 which include test

procedures for the following:

2. Referenced Documents

2.1 ASTM Standards: 2

D 412 Test Methods for Vulcanized Rubber and Thermo-

plastic Elastomers—Tension

D 624 Test Method for Tear Strength of Conventional

Vulcanized Rubber and Thermoplastic Elastomers

D 726 Test Method for Resistance of Nonporous Paper to

Passage of Air

D 737 Test Method for Air Permeability of Textile Fabrics

D 3675 Test Method for Surface Flammability of Flexible

Cellular Materials Using a Radiant Heat Energy Source

E 162 Test Method for Surface Flammability of Materials

Using a Radiant Heat Energy Source

E 662 Test Method for Speciﬁc Optical Density of Smoke

Generated by Solid Materials

These test methods are under the jurisdiction of ASTM Committee D20 on

Plastics and are the direct responsibility of Subcommittee D20.22 on Cellular

Materials-Plastics and Elastomers.

Current edition approved July 1, 2005. Published August 2005. Originally

approved in 1977. Last previous edition approved in 2003 as D 3574 – 03.

2For referenced ASTM standards, visit the ASTM website, www.astm.org, or

contact ASTM Customer Service at service@astm.org. For Annual Book of ASTM

Standards volume information, refer to the standard’s Document Summary page on

the ASTM website.

1

*A Summary of Changes section appears at the end of this standard.

Copyright © ASTM International, 100 Barr Harbor Drive, PO Box C700, West Conshohocken, PA 19428-2959, United States.

1

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

Tests:

Test A

Test B1

Test B2

Test C

Test D

Test E

Test F

Test G

Test H

Test I1

Test I2

Test I3

Test I4

Test J

Test K

Test L

Test M

Density Test

Indentation Force Deﬂection Test—Speciﬁed

Deﬂection

Indentation Force Deﬂection Test—Speciﬁed

Force

Compression Force Deﬂection Test

Constant Deﬂection Compression Set Test

Tensile Test

Tear Resistance Test

Air Flow Test

Resilience (Ball Rebound) Test

Static Force Loss Test at Constant Deﬂection

Dynamic Fatigue Test by the Roller Shear at

Constant Force,

Dynamic Fatigue Test by Constant Force

Pounding

Dynamic Fatigue Test for Carpet Cushion

Steam Autoclave Aging

Dry Heat Aging

Wet Heat Aging

Recovery Time

Sections

9-15

16-22

23-29

30-36

37-44

45-52

53-60

61-67

68-75

77-85

86-94

95-103

104-112

113-118

119-124

125-130

131-136

different parts of the ﬁnished product, especially if the article is

of complicated shape or of varying thickness, and these factors

affect the physical properties of the specimens. Also, the

density is affected by the number of cut surfaces on the

specimen. If a test specimen is die cut, sufficient time should be

allowed for complete recovery of the thickness across the full

width of the specimen.

7.3 When the ﬁnished molded product does not lend itself to

testing or to the taking of specimens because of complicated

shape, small size, metal or fabric inserts, adhesion to metal, or

other reasons, molded test slabs as agreed upon between the

supplier and the purchaser shall be prepared.

7.4 When differences in test results arise due to the difficulty

in obtaining suitable specimens from the ﬁnished parts, the

supplier and the purchaser may agree upon an acceptable

location to take the specimen.

8. Measurement of Test Specimens

8.1 Measure the length and width with a scale or tape. Take

care not to distort the foam.

8.2 Measure thickness up to and including 25 mm using a

dial-type gage with a minimum foot area of 650 mm2. Hold the

pressure of the dial foot to 170 6 35 Pa (Note 2). Thicknesses

over 25 mm may be measured with a dial gage, a sliding

caliper gage, or as speciﬁed in 8.1. When a sliding caliper gage

is employed, make the gage setting with the gage out of contact

with the foam. Pass the specimen through the previously set

gage: the proper setting shall be the one when the measuring

faces of the gage contact the surfaces of the specimen without

compressing it.

NOTE 2—For soft foams having compression force deﬂection values

less than 1.65 kPa, the pressure on the dial foot shall not exceed 100 Pa.

Appendixes:

X1. Suggested Method for Specifying Flexible Urethane Foams

X2. Suggested Method of Construction for a Roller Shear Dynamic Flex Fa-

tigue Apparatus

X3. Deﬁnitions of Terms Used to Describe the Force-Deﬂection Curve of

Flexible Urethane Foam

X4. Suggested Tests for Determining Combustibility of Flexible Urethane

Foam. (The combustion tests are given for informational purposes only

and are not part of the standard.)

X5. Suggested Method for Veriﬁcation of an Inclined Oil Manometer

X6. Suggested Method for Measuring Hysteresis Loss of Foams

5. Signiﬁcance and Use

5.1 The test procedures provide a standard method of

obtaining data for research and development, quality control,

acceptance and rejection under speciﬁcations, and special

purposes.

5.2 The data obtained by these test methods are applicable

to the material under conditions of the particular test and are

not necessarily the same as obtained in other environments in

use.

6. General Test Conditions

6.1 Tests shall be conducted under known conditions of

temperature and humidity or as speciﬁed in the individual test

procedure. The product shall be conditioned undeﬂected, and

undistorted at the temperature and humidity of test for at least

12 h before being tested. In cases of dispute, the tests shall be

made at a temperature of 23 6 2°C and in an atmosphere of 50

6 5 % relative humidity.

6.2 It is recommended for referee purposes that all tests

shall be performed 7 days or more after the foam has been

manufactured.

7. Sampling

7.1 When possible, the completed manufactured product

shall be used for the test speciﬁed. Representative samples of

the lot being examined shall be selected at random as required.

7.2 When it is necessary or advisable to obtain specimens

from the articles, as in those cases where the entire sample is

not required or adaptable for testing, the method of cutting and

the exact position from which specimens are to be taken shall

be speciﬁed. The density and the state of cure may vary in

2

8.3 The scale, tape, or gage shall be graduated so as to

permit measurements within 61 % of the dimensions to be

measured.

8.4 Unless otherwise speciﬁed, results shall be the mean of

the measurements.

TEST A—DENSITY TEST

9. Scope

9.1 This test method covers determination of the density of

uncored foam by calculation from the mass and volume of the

specimen. The density value thus obtained applies only to the

immediate area from which the specimen has been taken. It

does not necessarily relate to the bulk density of the entire

molded pad.

NOTE 3—ISO 845 is a similar test, but there are technical differences.

10. Test Specimen

10.1 Core Density—A representative specimen of regular

shape, circular or square without skins or densiﬁcation lines,

not less than 1000 mm3 in volume, shall be cut from a portion

free of voids and defects and as near as possible to the section

from which the tension and tear specimens were taken.

10.2 Section Density—A representative specimen with skins

on the top and bottom surface measuring at least 0.1 m2 in area

by full-part thickness shall be cut from an area free of voids

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

and defects and as near as possible to the location from which

the tension and tear specimens were taken. When these

dimensions are not possible, the largest representative portion

as agreed upon between the supplier and the purchaser shall be

used.

11. Number of Specimens

11.1 One specimen shall be tested, unless otherwise agreed

upon by the supplier and the purchaser.

12. Procedure

12.1 Determine the mass of the specimen within 1 %.

12.2 Determine the dimensions of the specimen in accor-

dance with Section 8, and calculate the volume.

13. Calculation

13.1 Calculate the density in kilograms per cubic metre as

follows:

Density 5 M/V 3 106

(1)

18. Test Specimen

18.1 The test specimen shall consist of the entire product

sample or a suitable portion of it, except that in no case shall

the specimen have dimensions less than 380 by 380 by 100

mm. Specimens less or different than 100 mm in thickness

shall have the thickness noted on the test report.

18.2 The IFD values for molded products are dependent on

the specimen dimensions. Higher values are generally obtained

for specimens that retain all molded surfaces.

19. Number of Specimens

19.1 One specimen shall be tested, unless otherwise agreed

upon by the supplier and the purchaser.

20. Procedure

20.1 Place the test specimen in position on the supporting

plate of the apparatus. If the product has one side cored or

honey-combed, this face shall rest on the perforated plate. The

specimen position shall be such that whenever practicable the

indentation will be made at the center of all articles, except

where another location is agreed upon by the supplier and the

purchaser.

20.2 Preﬂex the area to be tested by twice lowering the

indentor foot to a total deﬂection of 75 to 80 % of the full-part

thickness at a rate of 250 6 25 mm/min. Mark the location of

the test area with a pen by circumscribing the indentor foot

while under a 4.5-N force. Allow the specimen to rest 6 6 1

min after the preﬂex.

20.3 Bring the indentor foot into contact with the specimen

and determine the thickness after applying a contact force of

4.5 N (Note 5) to the indentor foot. Indent the specimen at 50

6 5 mm/min 25 % of this thickness and observe the force in

newtons after 60 6 3 s. Without removing the specimen

increase the deﬂection to 65 % deﬂection, allowing the force to

drift while maintaining the 65 % deﬂection, and again observe

the force in newtons after 60 6 3 s.

NOTE 5—For super-soft foam, foam with a 25 % IFD less than 40 N, a

reduction of pressure on the indentor foot shall be allowed. Sufficient

contact force to make an accurate initial thickness measurement is

required.

where:

M = mass of specimen, g, and

V = volume of specimen, mm3.

14. Report

14.1 Report the following information:

14.1.1 Density to the nearest 0.1 kg/m3, and

14.1.2 Type of specimen, core or section.

15. Precision and Bias

15.1 See Section 137 for Precision and Bias statements.

TEST B1 —INDENTATION FORCE DEFLECTION

TEST—SPECIFIED DEFLECTION

16. Scope

16.1 This will be known as the indentation force deﬂection

test and the results as the IFD values. This test consists of

measuring the force necessary to produce designated indenta-

tions in the foam product, for example, 25 and 65 % deﬂec-

tions. (Appendix X3).

NOTE 4—ISO 2439 is a similar test, but there are technical differences.

17. Apparatus

17.1 An apparatus having a ﬂat circular indentor foot 203

mm in diameter connected by means of a swivel joint capable

of accommodating the angle of the sample to a force-

measuring device and mounted in such a manner that the

product or specimen can be deﬂected at a speed of 50 to 500

mm/min. The apparatus shall be arranged to support the

specimen on a level horizontal plate which is perforated with

approximately 6.5-mm holes on approximately 20-mm centers

to allow for rapid escape of air during the test. Special support

for contoured molded pads shall be perforated in the same

manner as the ﬂat plate unless agreed upon between the

supplier and the purchaser. Pads longer than the base plate shall

be supported from distortion at the 4.5-N contact force.

3

21. Report

21.1 Report the force in newtons required for 25 and 65 %

indentation or other indentations (Note 6). These ﬁgures are

known as the 25 % and 65 % IFD values, respectively. Report

also length, width, and thickness of the specimen, if non-

standard and the ratio (support factor Appendix X3) of 65 % to

25 % IFD values.

NOTE 6—Indentation deﬂection tests, other than 25 and 65 %, as well as

a 25 % return value (25 % RT), may be speciﬁed as agreed upon between

the supplier and the purchaser.

22. Precision and Bias

22.1 See Section 137 for Precision and Bias statements.

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

TEST B2 —INDENTATION RESIDUAL GAGE

LENGTH TEST—SPECIFIED FORCE

23. Scope

23.1 Cellular foam products have been traditionally checked

for indentation force deﬂection by determining the force

required to effect a 25 % deﬂection. In seating, on the other

hand, the interest is in determining how thick the padding is

under the average person. Two measurements are called for to

meet the requirements of this test method. The force deﬂection

is determined by measuring the thickness of the pad under a

ﬁxed force of 4.5 N, 110 N, and 220 N, on a 323-cm2 circular

indentor foot.

23.2 This determination shall be known as the Indentation

Residual Gage Length and the measurements as the IRGL

values.

NOTE 7—ISO 2439 is a similar test, but there are technical differences.

27.3 Apply the 110-N force at 50 6 5 mm/min with the

indentor foot and indent the specimen until the force is carried

by the specimen. Determine the thickness at 110 N after

maintaining the force for 60 6 3 s.

27.4 Without removing the specimen apply the 220-N force

at 50 6 5 mm/min with the indentor foot and further indent the

pad until this load is carried. After 60 6 3 s under load,

determine the thickness of the pad.

28. Report

28.1 Report the specimen thickness after 60 6 3 s at 4.5 N,

110 N, and 220 N. These ﬁgures are known as the IRGL values,

respectively. Report also the length, width, and thickness of the

specimen.

29. Precision and Bias

29.1 See Section 137 for Precision and Bias statements.

TEST C—COMPRESSION FORCE DEFLECTION

TEST

30. Scope

30.1 This test consists of measuring the force necessary to

produce a 50 % compression over the entire top area of the

foam specimen.

NOTE 8—ISO 3386 is a similar test, but there are technical differences.

NOTE 9—Compression deﬂection tests other than at 50 % may be

speciﬁed as agreed upon between the supplier and the purchaser.

24. Apparatus

24.1 An apparatus having a ﬂat circular indentor foot 203

mm in diameter connected with a swivel joint for applying

forces of 4.5 N, 110 N, 220 N and 330 N shall be mounted over

a level horizontal platform that is perforated with approxi-

mately 6.5-mm holes on approximately 20-mm centers to

allow for rapid escape of air during the test. The distance

between the indentor foot and the platform shall be variable to

indent the specimen at a speed of 50 to 200 mm/min for

thickness measurements. The apparatus shall be equipped with

a device for measuring the distance between plates.

24.2 Special support for contoured molded pads shall be

perforated and agreed upon between the supplier and the

purchaser. Pads longer than the base plate shall be supported

from distortion at the 4.5-N contact force.

25. Test Conditions

25.1 When possible the completed manufactured product

shall be used. In the case of tapered cushions, the location of

the area for measurement is to be agreed upon between the

supplier and the purchaser. In the case a ﬁnished part is not

feasible for test, 380 by 380-mm specimens of an average

thickness are to be cut from the cushion.

25.2 The IRGL values for molded products are dependent

on the specimen dimensions. Difference values are generally

obtained for specimens that retain all molded surfaces.

26. Number of Specimens

26.1 One specimen shall be tested, unless otherwise agreed

upon by the supplier and the purchaser.

27. Procedure

27.1 Test the whole test specimen or a minimum area of 380

by 380 mm. Preﬂex the specimen twice with a 330 N force at

200 6 20 mm/min. Allow to rest 6 6 1 min. Position the

specimen in the test apparatus with any cored or convoluted

surfaces resting against the perforated bottom plate.

27.2 Bring the indentor foot into contact and determine the

thickness of the specimen with the 4.5-N load on the indentor

foot.

4

31. Apparatus

31.1 An apparatus having a ﬂat compression foot, larger

than the specimen to be tested connected to a force-measuring

device and mounted in a manner such that the product or

specimen can be deﬂected at a speed of 50 to 500 mm/min. The

apparatus shall be arranged to support the specimen on a level

horizontal plate that is perforated with approximately 6.5-mm

holes on approximately 20-mm centers to allow for rapid

escape of air during the test.

32. Test Specimens

32.1 The slab test specimen shall have parallel top and

bottom surfaces and essentially vertical sides. The thickness

shall be no greater than 75 % of the minimum top dimension.

The standard specimen shall be 50 mm by 50 mm by 25 mm

in thickness.

32.2 Specimens from uncored slab stock shall be a mini-

mum of 2000 mm2 in area and have a minimum thickness of 20

mm.

32.3 The test specimen from molded parts shall have

parallel top and bottom surfaces and perpendicular sides.

Preferably the specimen should include both top and bottom

molded skins. If a test specimen with parallel top and bottom

surfaces including both molded skins cannot be obtained

because of the shape of the molded part, at least one of the

molded skin surfaces should be retained. Both surface skins

should be removed only in cases where the shape of the

original sample makes this absolutely necessary.

32.4 Maximum molded specimen thickness shall be no

greater than the minimum top dimensions. Specimens from

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

molded parts shall be a minimum of 2000 mm2 in area and

have a minimum thickness of 20 mm.

33. Number of Specimens

33.1 Three specimens per sample shall be tested. The value

reported shall be the mean value of those observed.

34. Procedure

34.1 Preﬂex the specimen twice, 75 to 80 % of its original

thickness at 250 6 25 mm/min. Then allow the specimen to

rest for a period of 6 6 1 min.

34.2 Place the specimen centered in the line of the axial load

on the supporting plate of the apparatus. If the product has one

side cored or convoluted, rest this face on the perforated plates.

34.3 Bring the compression foot into contact with the

specimen and determine the thickness after applying a contact

load of 140 Pa to the specimen area (Note 2). Compress the

specimen 50 % of this thickness at 50 6 5mm/min and

determine the ﬁnal force after 60 6 3 s.

35. Report

35.1 Report the thickness after contact force, and the 50 %

compression deﬂection value in kilopascals and the dimensions

of non-standard specimens. Indicate if the sample was cored or

convoluted.

36. Precision and Bias

36.1 See Section 137 for Precision and Bias statements.

TEST D—CONSTANT DEFLECTION COMPRESSION

SET TEST

37. Scope

37.1 This test method consists of deﬂecting the foam

specimen to a speciﬁed deﬂection, exposing it to speciﬁed

conditions of time and temperature and measuring the change

in the thickness of the specimen after a speciﬁed recovery

period.

NOTE 10—ISO 1856 is a similar test, but there are technical differences.

39.5 Specimens greater than 50 mm in thickness shall be cut

to 25 mm thickness from the core. (Note 11)

NOTE 11—Specimens from molded products may be tested with one or

both skins by agreement between the customer and the supplier.

40. Number of Specimens

40.1 Three specimens per sample shall be tested. The value

reported shall be the mean of those observed.

41. Procedure

41.1 Perform the entire test procedure under the following

conditions: Conduct all measurements, conditioning, and re-

covery of the specimen at 23 6 2°C and in an atmosphere of

50 6 5 % relative humidity. The oven conditions shall be 70 6

2°C and 6 % maximum relative humidity.

NOTE 12—This condition of relative humidity may be achieved by

placing an oven at 70 6 2°C in an atmosphere maintained at 23 6 2°C and

50 6 5 % relative humidity.

41.2 Measure the original thickness of the test specimen in

accordance with the procedure described in Section 8.

41.3 Place the test specimen in the apparatus and deﬂect it

to either 50 6 1, 75 6 1, or 90 6 1 % of its thickness, or any

other deﬂection agreed upon between the supplier and the

purchaser.

41.4 Within 15 min, place the deﬂected specimen and the

apparatus in the mechanically convected air oven for a period

of 22 h; then remove the apparatus.

41.5 Remove the specimen immediately from the apparatus

and measure the ﬁnal thickness in accordance with the proce-

dure described in Section 8 after allowing it to recover 30 to 40

min at the temperature and humidity conditions speciﬁed in

41.1.

NOTE 13—Recovery periods greater than 30 to 40 min may be agreed

upon by the supplier and the purchaser.

42. Calculation

42.1 Calculate the compression set value by one of the

following formulas:

NOTE 14—The Ct calculation is preferred and shall be the calculation

used when neither Ct and Cd are speciﬁed.

38. Apparatus

38.1 Compression Device, consisting of two or more ﬂat

plates arranged so the plates are held parallel to each other by

bolts or clamps and the space between the plates is adjustable

to the required deﬂection thickness by means of spacers.

39. Test Specimens

39.1 The test specimens shall have parallel top and bottom

surfaces and essentially perpendicular sides.

39.2 Specimens shall be 50 by 50 by 25 mm unless

otherwise speciﬁed. Specimens less than 25 mm in thickness

shall be plied up, without the use of cement, to a 25-mm

thickness.

39.3 Specimens from cored foams shall have a minimum

top surface area of 100 cm2. The thickness shall be no greater

than 75 % of the minimum top dimension.

39.4 Specimens from uncored molded products 25 mm or

less in thickness shall be 50 by 50 mm by full-part thickness

and shall contain the top and bottom skin.

5

42.1.1 Calculate the constant deﬂection compression set,

expressed as a percentage of the original thickness, as follows:

Ct 5 [~to 2 tf!/to # 3 100

(2)

where:

Ct = compression set expressed as a percentage of the

original thickness,

to = original thickness of test specimen, and

= ﬁnal thickness of test specimen.tf

42.1.2 Calculate the constant deﬂection compression set,

expressed as a percentage of the original deﬂection, as follows:

Cd 5 [~to 2 tf!/~to 2 ts!# 3 100

(3)

where:

Cd = compression set expressed as a percent of the origi-

nal deﬂection,

= original thickness of test specimen,to

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

ts

tf

= thickness of spacer bar used, and

= ﬁnal thickness of test specimen.

generally are unsuitable for ﬂexible foam. For testing dumbbell

specimens, the machine shall have either screw-type ﬂat plate

grips or a type of grip that tightens automatically and exerts a

uniform pressure across the gripping surfaces, increasing as the

tension increases to prevent slipping.

47. Test Specimens

47.1 The test specimens shall be cut from ﬂat sheet material

12.5 6 1.5 mm thick. The foam rise shall be in the thickness

direction, unless otherwise agreed upon by customer and

supplier. The top and bottom surfaces shall be parallel and free

of skin. The cut edges shall be perpendicular to the top surface

and be free of ragged edges. The length of the tabs may be

adjusted to ﬁt machine conditions provided that all other

requirements remain constant.

48. Number of Specimens

48.1 Three specimens per sample shall be tested. The value

reported shall be the mean value of those observed.

49. Procedure

49.1 Set the grip separation at a minimum of 62.5 mm for

the D 3574 Die and at a minimum of 75 mm for the D 412 Die

A. Place the dumbbell tabs in the grips of the testing machine,

using care to adjust them symmetrically, in order that the

tension will be distributed uniformly over the cross section.

The test shall be run at a speed of 500 6 50 mm/min, unless

otherwise speciﬁed by agreement between customer and sup-

plier. Start the machine and note continuously the distance

between the two bench marks. Record the stress at the

corresponding elongation or if an automatic recording device is

used, it will record the data continuously. At rupture, measure

or record elongation to the nearest 10 %.

50. Calculation

50.1 Calculate the tensile strength by dividing the maximum

breaking force by the original cross-sectional area of the

specimen.

50.2 Calculate the stress by dividing the force at a prede-

termined elongation by the original cross-sectional area of the

specimen.

50.3 Calculate the ultimate elongation, A, by subtracting the

original distance between the bench marks from the total

distance between the bench marks at the time of rupture and

expressing the difference as a percentage of the original

distance, as follows, or use the grip separations in a similar

calculation.

A, % 5 [~df 2 do!/do # 3 100

(4)

NOTE 15—Approximate conversion of Ct to Cd can be calculated by

multiplying the 50 % Ct by 2, the 75 % Ct by 1.33, and the 90 % Ct by

1.11.

43. Report

43.1 Report compression set as Ct or Cd, and deﬂection

used. Also report any non-standard recovery periods or sample

sizes and whether the sample was cored, uncored and/or

molded.

44. Precision and Bias

44.1 See Section 137 for Precision and Bias statements.

TEST E—TENSILE TEST

45. Scope

45.1 This test method determines the effect of the applica-

tion of a tensile force to foam. Measurements are made for

tensile stress, tensile strength, and ultimate elongation.

NOTE 16—ISO 1798 is a similar test, but there are technical differences.

46. Apparatus

46.1 Specimens—The specimen for tensile tests shall be

stamped out with a die of the shape and dimensions shown in

Fig. 1, or Die A of Test Methods D 412. The die shall be sharp

and free of nicks in order to prevent leaving ragged edges on

the specimen. The D 412 Die is the preferred die and is

identical in dimensions to the ISO 1798 Die.

46.2 Bench Marker—The marker shall have two parallel

marking edges 1 to 3 mm in thickness and spaced 20 or 25 mm

apart on centers.

46.3 Measurements—The dimensions of the test specimen

shall be determined with a suitable gage in accordance with

Section 8.

46.4 Machine—Tensile tests shall be made on a power-

driven machine complying with the following requirements:

46.4.1 The machine shall be equipped with a load cell or

force measuring device that can measure the maximum applied

force. The test speed shall be 500 6 50 mm/min, and shall be

uniform at all times.

46.4.2 The machine may be equipped with a device gradu-

ated to 2.5 mm for measuring the elongation. The use of

non-contact extensometers may similarly be used for determin-

ing elongation. Extensometers that clip on to the specimen

where:

do = original distance between bench marks, and

df = distance between bench marks at the break point.

50.4 The value reported shall be the mean value of all

specimens tested.

51. Report

51.1 Report the following information:

51.1.1 Tensile strength in kilopascals,

6

FIG. 1 Die for Stamping Tension Specimens

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

51.1.2 Stress in kilopascals at a predetermined elongation,

and

51.1.3 Ultimate elongation, in percent, and whether bench

marks, grip separation or extensometers were used to measure

elongation.

51.1.4 Crosshead speed, if other than 500 mm/min.

52. Precision and Bias

52.1 See Section 137 for Precision and Bias statements.

TEST F—TEAR RESISTANCE TEST

53. Scope

53.1 This test method covers determination of the tear

propagation resistance of foam. The block method, as de-

scribed, measures the tear resistance under the conditions of

this particular test.

NOTE 17—ISO 8067 is a similar test, but there are technical differences.

18). After the rupture of the specimen, or after at least a 50-mm

length is torn, record the maximum force in Newtons and note

also the thickness of the specimen (direction A-B).

NOTE 18—For foams that will not tear by this method side by side tear

strength comparisons can be made by testing in accordance with Test

Method D 624. It should be noted that the D 624 test is a tear initiating

measurement as opposed to a tear propagating measurement in this block

tear test.

58. Calculation

58.1 Calculate the tear strength from the maximum force

registered on the testing machine and the average thickness of

the specimen (direction A-B), as follows:

Tear strength, N/m 5 F/T 3 103

(5)

where:

F = force, N, and

T = thickness, mm.

59. Report

59.1 Report the following information:

59.1.1 Tear strength in newtons per metre,

59.1.2 Orientation of specimen, and

59.1.3 Crosshead speed, if other than 500 mm/min.

60. Precision and Bias

60.1 See Section 137 for Precision and Bias statements.

TEST G—AIR FLOW TEST

61. Scope

61.1 The air ﬂow test measures the ease with which air

passes through a cellular structure. Air ﬂow values may be used

as an indirect measurement of certain cell structure character-

istics. The test consists of placing a ﬂexible foam core

specimen in a cavity over a chamber and creating a speciﬁed

constant air-pressure differential. The rate of ﬂow of air

required to maintain this pressure differential is the air ﬂow

value This test is normally for slab foam products or for the

core materials of molded products. Measurements of air ﬂow

through molded skins or extremely high air ﬂow products may

require alternative methods (Note 20).

NOTE 19—ISO 7231 is an identical test.

NOTE 20—For measuring air ﬂow of products, such as viscoelastic

foams, which can have air ﬂows beyond the range of this method, success

has been achieved using the equipment speciﬁed in Test Method D 737.

Some modiﬁcation of the equipment may be necessary.3 For surface

porosity of molded foams see Test Method D 726.

54. Apparatus

54.1 Tear resistance shall be measured on a power-driven

apparatus which will indicate the force at which rupture of the

specimen takes place. An automatic machine may be used

which draws the actual curve, or, a style or scale shall be used

having an indicator that remains at the point of maximum force

after rupture.

55. Test Specimens

55.1 The test specimens shall be a block shape free of skin,

voids, and densiﬁcation lines, as shown in Fig. 2. They may be

cut on a saw or die cut from sheet material so that the sides are

parallel and perpendicular to each other. A nominal 40-mm cut

shall be placed in one side as shown in Fig. 2. Dimension A-B

can be reduced to the pad thickness. The thickness shall be

determined in accordance with Section 8.

56. Number of Specimens

56.1 Three specimens per sample shall be tested. The values

reported shall be the mean of those tested.

57. Procedure

57.1 Clamp the test specimen in the jaws of the testing

machine, taking care that the jaws grip the specimen properly.

Spread the block so that each tab is held in the jaw to pull

across the specimen. The test shall be run at a speed of 500 6

50 mm/min, unless otherwise speciﬁed by agreement between

customer and supplier. Aid the cut in the specimen with a razor

blade or knife, so as to keep it in the center of the block (Note

62. Terminology

62.1 Deﬁnitions of Terms Speciﬁc to This Standard:

62.1.1 air ﬂow value—the volume of air per second at

standard temperature and atmospheric pressure required to

maintain a constant pressure differential of 125 Pa across a

ﬂexible foam specimen approximately 50 by 50 by 25 mm.

FIG. 2 Tear Resistance Test Specimens

Gummaraju, R.V., Pask, R.F., Koller, H.J., Wujcik, S.E., and Reimann, K.A.,

“Evaluation, Modiﬁcation and Adaptation of an Airﬂow Test Method for Polyure-

thane Foams,” Journal of Cellular Plastics, May/June 2001.

3

7

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

FIG. 3 Air Flow Apparatus Schematic Diagram

62.1.2 air ﬂow parallel to foam rise—the air ﬂow value

obtained when the air enters and leaves the mounted specimen

parallel to foam rise.

62.1.3 air ﬂow perpendicular to foam rise—the air ﬂow

value obtained when the air enters and leaves the specimen

perpendicular to foam rise.

63. Apparatus

63.1 A schematic drawing of the apparatus including the

specimen mounting chamber, manometer, air ﬂowmeters,

blowmeters, blower, and voltage control is shown in Fig. 3.4

63.2 Chamber, consisting of a pot approximately 130 mm in

diameter and 150 mm high with provision for mounting the

foam specimen and ﬁttings for the manometer and air exhaust.

The specimen mount cavity shall be 50.0 6 0.5 by 50.0 6 0.5

by 25.0 6 0.5 mm in size. Four foam support vanes approxi-

mately 1 mm thick and 12.5 mm high shall be placed under the

opening to prevent the foam from being pulled into the vacuum

chamber. The vanes shall be spaced 12.5 mm on center from

each other and also centered relative to the bottom of the cavity

opening. The manometer ﬁtting shall enter a 1-mm hole

The sole source of supply of an electronic instrument that has proven to be

effective for measuring air ﬂow, which is known to the committee at this time is

ONIX Process Analysis, Inc., 1201 N. Velasco, Angleton, TX 77515. If you are

aware of alternative suppliers, please provide this information to ASTM Interna-

tional Headquarters. Your comments will receive careful consideration at a meeting

of the responsible technical committee,1 which you may attend.

4

midway along the side of the chamber. A 25-mm pipe ﬁtting

shall be used as the exhaust outlet from the center of the bottom

of the chamber.

63.3 Manometer, calibrated from 0 to 250 Pa and having an

accuracy of 62 %, is required. An inclined oil manometer with

graduations of 2 Pa is recommended. A level mounted on the

manometer shall be used to ensure that the proper degree of

inclination from the horizontal is maintained. Traps shall be

provided to prevent indicating ﬂuid from being accidentally

drawn into the chamber. Appendix X5. describes a suggested

method for the veriﬁcation of the inclined oil manometer, the

manometer can alternatively be replaced with a 0-250 Pa

magnehelic gage with graduations in 5 Pa.

63.4 Flowmeters and Blower—Low-pressure-drop air ﬂow-

meters accurate to 62 % shall be used for air-ﬂow measure-

ments. A given ﬂowmeter should not be used for values less

than 10 % of full scale. Air ﬂowmeters with at least 250-mm

scales are recommended. Since the ﬂowmeter calibration is

temperature-and pressure-dependent, the use of the apparatus

under ambient conditions can result in erroneous readings. In

cases of dispute, the apparatus should be used under standard

conditions of 23°C and 100 kPa (1 atm pressure) or else a

suitable calibration correction applied. Flowmeters that range

from 0 to 0.01 m3 /s will cover a wide range of foam cell

structures but a lesser range may be used. Actual ﬂow is

adjusted by a combination of valve restriction and blower

speed. The two-way valves shall be mounted on the output side

8

D 3574 – 05

of the ﬂowmeter to maintain the pressure drop across the

ﬂowmeter constant at any given ﬂow level. A vacuum cleaner

type unit shall be used for an exhaust blower.

63.5 Leak Test—To check the apparatus for leaks, the

specimen mount cavity shall be sealed with masking tape. With

all valves closed, turn on the exhaust blower to approximately

1⁄3 power and observe any movement of the manometer. The

manometer reading, if any, should not exceed 1 Pa after a 30-s

waiting period. Next, open the valve very slightly for the

lowest range ﬂowmeter reading. The ﬂow should be essentially

zero as evidenced by less than 3-mm movement of the air

ﬂowmeter ﬂoat from its static position. For the equipment to

perform satisfactorily over its entire range the requirements for

both parts of the leak test must be met.

64. Test Specimens

64.1 The test specimens shall be parallel-piped cut to ﬁt the

mount cavity of the apparatus. A cavity 50 by 50 mm requires

a specimen 51.0 6 0.3 by 51.0 6 0.3 by 25.0 6 0.5 mm in size.

A band saw with a movable table and a double-bevel knife-

edge blade is recommended for cutting the specimens.

64.2 Three specimens per sample for each location and

orientation to be tested shall be cut. The values reported shall

be the mean of those observed for each location and orienta-

tion.

65. Procedure

65.1 Measure each specimen in accordance with the proce-

dure described in Section 8 to verify the specimen size.

65.2 Insert the specimen into the test cavity. Make sure that

a good air seal is obtained along all edges. The top of the

specimen should be ﬂush with the top of the test chamber.

65.3 With all valves closed, adjust the voltage control of the

apparatus to 30 %.

65.4 Open one ﬂow-control valve slowly until a pressure

differential to 100 to 150 Pa is obtained. Adjust the voltage

control carefully to obtain a pressure differential of 125 6 1 Pa.

65.5 After this pressure differential has been maintained for

at least 10 s, read the scale of the ﬂowmeter.

65.6 If this reading is off-scale or less than 10 % of full

scale, close that ﬂow-control valve and open a more appropri-

ate one. Repeat this process until the proper manometer

reading and air ﬂow is achieved.

65.7 The air ﬂow value may be obtained from the ﬂowmeter

scale directly, estimated from a calibration chart, or calculated

with a factor depending on the calibration system.

66. Report

66.1 Report the following information:

66.1.1 Location and orientation of each specimen with

respect to foam rise in the section of foam that was sampled,

66.1.2 Mean air ﬂow value in cubic metres per min for each

location and orientation,

66.1.3 Dimensions of the specimen, and

66.1.4 Dimension of the mount cavity of the apparatus.

67. Precision and Bias

67.1 See Section 137 for Precision and Bias statements.

9

TEST H—RESILIENCE (BALL REBOUND) TEST

68. Scope

68.1 This test consists of dropping a steel ball on a foam

specimen and noting the height of rebound.

NOTE 21—ISO 8307 is an identical test.

69. Apparatus

69.1 The ball rebound tester shall consist of a 40 6 4-mm

inside diameter vertical clear plastic tube, such as acrylic, into

which a 16.03 6 0.2-mm diameter steel ball is released by a

magnet or other device. The steel ball must be released so that

it falls without rotation. Centering of the ball is assured by a

recess at the base of the magnet. The height of drop shall be

500 mm. Since it is most convenient to note the position of the

top of the ball on rebound, the top of the ball shall be 516 mm

above the surface of the foam. Thus, “zero” rebound shall be

16.3 6 0.2 mm (diameter of ball) above the specimen surface.

The scale on the tube shall be scribed directly in percent as

follows. Every 5 % a complete circle shall be scribed and every

1 % a 120° arc shall be scribed. The complete circles are an

essential part of the apparatus, since they are used to eliminate

parallax error.

70. Test Specimens

70.1 The test specimens shall have parallel top and bottom

surfaces.

70.2 The test specimens shall consist of the entire product

sample or a suitable portion of it, except that in no case shall

the thickness be less than 30 mm. The standard specimen size

shall be 100 mm by 100 mm by 50 mm. For molded products

the top skin shall be removed.

71. Number of Specimens

71.1 Three specimens per sample shall be tested. The three

specimens may be obtained by using separate items or different

locations on a given item.

72. Procedure

72.1 Center the specimen at the base of the tube and adjust

the height of the tube so that zero rebound is 16 mm above the

surface of the foam specimen.

72.2 Mount the steel ball on the release mechanism; then

drop it and note the maximum rebound height. If the ball

strikes the tube on the drop or rebound, the value obtained is

invalid. This condition is usually due to the tube not being

vertical or irregularities on the specimen surface. In order to

minimize parallax error, the circles on the tube in the region

where the percent rebound is read must appear as lines.

72.3 Make an additional two drops on the same specimen in

the same location unless agreed upon by customer and supplier.

73. Calculation

73.1 Calculate the mean of the three rebound values.

74. Report

74.1 Report the mean of the three specimen mean values as

the ball rebound resilience value of the sample in percent.

D 3574 – 05

74.2 Report if measurements were made at different speci-

men locations or on different specimens.

75. Precision and Bias

75.1 See Section 137 for Precision and Bias statements.

TEST I—FATIGUE TESTS

76. Scope

76.1 The fatigue tests consist of four methods:

76.1.1 Static Force Loss Test at Constant Deﬂection,

76.1.2 Dynamic Fatigue by Roller Shear at Constant Force,

76.1.3 Dynamic Fatigue Test by Constant Force Pounding,

and

76.1.4 Dynamic Fatigue Test for Carpet Cushion.

TEST I1 —STATIC FORCE LOSS TEST AT

CONSTANT

DEFLECTION

77. Scope

77.1 The purpose of this static force loss test is to deter-

mine: (1) a loss of IFD, (2) a loss of thickness, and (3)

structural breakdown by visual examination.

77.2 This procedure tests the specimen at a 75 % constant

deﬂection.

NOTE 22—No similar ISO standard exists.

82.3 For a measurement of more permanent fatigue, repeat

82.1, except allow 24 6 1 h of recovery time rather than 60

min.

83. Calculation and Inspection

83.1 Check the specimen for physical breakdown of the

cellular structure by visual examination and comparison with

unﬂexed specimens.

83.2 Calculate the percentage loss of thickness as follows:

Ft 5

~to 2 tf !

3 100

~to !

(6)

where:

Ft = loss in thickness, %,

to = original specimen thickness, and

tf = ﬁnal specimen thickness.

83.3 Calculate the percentage loss of IFD, as follows:

FL 5

~Lo 2 Lf !

3 100

~Lo !

(7)

where:

FL = loss of indentation force deﬂection, %,

Lo = original indentation force deﬂection value, and

Lf = ﬁnal indentation force deﬂection value.

84. Report

84.1 Report the following information:

84.1.1 Percentage loss of thickness and the percentage loss

of 25 and 65 % IFD if the thickness loss is less than 10 %, and

84.1.2 Results of visual examination.

84.1.3 Recovery time whether 60 min or 24 h.

85. Precision and Bias

85.1 Round robin testing to determine the precision of this

method is being planned and the data will be available by the

end of 2006.

78. Apparatus

78.1 The apparatus shall consist of two parallel plates

(wood or metal) which can produce a uniform, constant

deﬂection of the specimen. The plates shall be 500 by 500 mm

square, and spacer bars or other appropriate means shall be

employed to maintain a constant 75 % deﬂection throughout

the test.

79. Test Specimen

79.1 The test specimen shall be 380 by 380 mm by the

desired thickness. One specimen shall be tested.

80. Initial Measurements

80.1 Measure the 25 and 65 % IFD of the test specimen in

accordance with Sections 16 to 22. Measure the original

thickness with 4.5-N contact force after preﬂexing.

81. Procedure

81.1 Place the specimen between the plates with the spacer

bars to provide a 75 % deﬂection. Clamp the plates and hold at

75 % deﬂection for 22 h at 23 6 2°C and 50 6 5 % relative

humidity.

82. Final Measurements

82.1 Measure the ﬁnal IFD values 60 6 5 min after the

fatigue test is completed in accordance with 80.1 using the

original thickness to determine the deﬂection for the ﬁnal IFD

values.

82.2 If the loss in thickness is above 10 %, the IFD losses

shall not be measured and only the thickness loss shall be

reported.

10

TEST I2 —DYNAMIC FATIGUE TEST BY THE

ROLLER

SHEAR AT CONSTANT FORCE

86. Scope

86.1 This procedure fatigues the specimen dynamically at a

constant force, deﬂecting the material both vertically and

laterally.

86.2 The fatigue test may be conducted by either Procedure

A or Procedure B. Both test procedures are the same and differ

only in the number of cycles used. Procedure A shall use 8000

cycles (approximately 5 h) and Procedure B shall use 20 000

cycles (approximately 12 h).

NOTE 23—No similar ISO standard exists.

NOTE 24—The mass of the roller and the number of cycles may be

changed as agreed upon between the supplier and the purchaser.

D 3574 – 05

87. Apparatus (Appendix X2)

87.1 Perforated-Base Platen, approximately 500 by 500 by

10 mm with a ﬁnished ground-top surface and with perforation

of approximately 6.5-mm centers covering the center 360 by

360-mm portion.

87.2 Roller, 450-mm minimum length and 76.0 6 1.3

mm-diameter made from stainless steel or chrome-plated metal

having a minimum surface ﬁnish of 1 µm. The roller shall be

mounted in an offset position (15 6 3°) with suitable means of

adjustment for a speciﬁed loading of the test specimen. The

force imparted by the roller assembly shall not exceed 110 N.

87.3 The test is conducted at a frequency of 0.50 6 0.05 Hz.

A cycle is a complete forward and reverse stroke. The length of

the stroke shall be 300 6 10 mm.

87.4 Any suitable method for holding the test specimen

securely on the roller base platen is acceptable as long as the

test specimen remains stationary during the rolling ﬂex cycles.

An acceptable method for retaining the specimen on the base

platen is described as follows: Four pieces of cotton sheeting or

paper masking tape 50 to 75 mm wide at least 50 mm longer

than each side of the test specimen shall be required. Bond the

cotton strips (with a solvent or water-emulsion-type of adhe-

sive) or the masking tape along the edges of the base surface of

the test specimen. Allow 25 to 50 mm of each strip to extend

beyond the edges of the test specimen so that the test specimen

can be securely clamped to the base platen through the use of

suitable metal retainer straps.

88. Test Specimen

88.1 A specimen 380 mm long by 300 mm wide by 50 mm

thick is used. The thickness of specimens tested should be at

least 25 mm and no greater than 125 mm. Normally full-part

thickness is used where the top and bottom surfaces are

essentially parallel and fall within the thickness limits. Where

part thickness exceeds 125 mm or the bottom surface is

contoured so that the surfaces are not essentially parallel, the

bottom surface shall be sliced to provide a ﬂat surface

essentially parallel to the top surfaces (see Section 7).

88.2 The length and width dimensions shall be held to 66.5

mm and shall be saw cut or die cut; if die cut, sufficient time

must be allowed for complete edge recovery (usually 2 h

minimum).

88.3 One specimen shall be tested, unless otherwise agreed

upon by the supplier and the purchaser.

89. Initial Measurements

89.1 Bond the masking tape or suitable hold-down cloth to

the bottom edges of the specimen so the specimen can be

secured to the perforated base platen of the fatigue tester.

89.2 Condition the specimen as in Section 6. The test should

also be run under the same conditions.

89.3 Determine the IRGL in accordance with Sections

23-29.

90. Procedure

90.1 Adjust the roller to obtain a constant force of 130 6 2

N on the foam specimen (Note 24). This critical measurement

may be made by fashioning a lightweight fabric sling around

11

the roller at its center and measuring the force downward while

holding the weighing scale vertically over the roller and

maintaining the roller axis in a horizontal plane with the pivot

axis.

90.2 Set the vertical adjustment of the roller or the mounting

base by placing the specimen in position and lowering the

roller so it is supported by the specimen. Observe the pivot axis

and roller axis relationship and adjust the vertical height so that

the axes lie in an essentially horizontal plane at the start of the

test.

90.3 Mount the test specimen on the base platen with the

long dimension parallel to the stroke of the dynamic fatigue

machine and secure by means of the tape and metal-retainer

strips. When mounting cored pieces, coring is to be against the

platen. Set the counter to zero, start the machine, and fatigue

test the sample for either 8000 cycles (Procedure A) or 20 000

cycles (Procedure B) or another number of cycles speciﬁed by

the customer.

91. Final Measurements

91.1 Within 60 6 5 min after the fatigue test is completed,

measure the ﬁnal IRGL in accordance with 89.3.

91.2 For a measurement of more permanent fatigue repeat

91.1, except allow 24 6 1 h of recovery rather than 60 min.

92. Calculation and Inspection

92.1 Check the specimen for physical breakdown of cellular

structure by visual examination and comparison with unﬂexed

similar specimens.

92.2 Calculate and report the percent loss in thickness as

follows:

Thickness loss, % 5

@100~A 2 B!#

~A!

(8)

where:

A = original thickness under compression forces of 4.5 N,

110 N, and 220 N, and

B = ﬁnal thickness under the same indentation forces.

92.3 If requested by the customer, calculate the total loss

number as follows:

Total loss number 5 sum of % losses at each load

Sample Calculation:

Percent thickness loss at 4.5 N = 2.0

Percent thickness loss at 110 N = 18.0

Percent thickness loss at 220 N = 27.0

Total loss number 47.0

(9)

93. Report

93.1 Report the following information:

93.1.1 Percentage loss of thickness and IRGL values.

93.1.2 The number of cycles.

93.1.3 Total loss number, if requested.

93.1.4 Results of visual examination.

93.1.5 Recovery time whether 60 min or 24 h.

94. Precision and Bias

94.1 Round robin testing to determine the precision of this

method is being planned and the data will be available by the

end of 2006.

D 3574 – 05

TEST I3 —DYNAMIC FATIGUE TEST BY CONSTANT

FORCE POUNDING

95. Scope

95.1 The purpose of the fatigue test is to determine: (1) the

loss of force support at 40 % IFD (indentation force deﬂec-

tion), (2) a loss in thickness, and (3) structural breakdown as

assessed by visual inspection. Deﬂections other than 40 % may

be used as agreed upon between supplier and purchaser.

95.2 This procedure describes tests that evaluate the speci-

men by repeatedly deﬂecting the material by a ﬂat-horizontal

indention exerting a vertical force of 750 6 20 N on the test

specimen.

95.3 This fatigue test may be conducted by Procedure A,

Procedure B, or Procedure C. Procedures A and B differ only

in the number of cycles used. Procedure A shall use 8000

cycles (approximately 2 h) and Procedure B shall use 80 000

cycles (approximately 19 h). Procedure C calls for 12 000

cycles at a slower cycling rate (approximately 20 h). See 96.3.

NOTE 25—The equipment in this standard is identical to ISO 3385, but

there are technical differences in the two methods.

8000 cycles (Procedure A), 80 000 cycles (Procedure B), or

12 000 cycles (Procedure C). Procedure C shall be used for

slow recovery (viscoelastic) foams where the cycle speed is

slow enough to allow enough time between cycles for the foam

to recover its height.

100. Final Measurement

100.1 Within 60 6 5 min after the fatigue test is completed,

repeat 98.2 using the original thickness to determine the

deﬂection for the ﬁnal force reading.

100.2 For a measurement of more permanent fatigue repeat

100.1, except allow 24 6 1 h of recovery rather than 60 min.

100.3 If the loss in thickness is above 10 %, IFD loss shall

not be measured and only the thickness loss should be reported.

101. Calculation and Inspection

101.1 Check the specimen for physical breakdown of the

cellular structure by visual examination and comparison with

unﬂexed specimens.

101.2 Calculate the percent loss of thickness as follows:

Ft 5

~to 2 tf !

3 100

~to !

(10)

96. Apparatus

96.1 Perforated Base Platen, approximately 500 by 500 by

10 mm, with ﬁnished ground-top surface and with perforation

of approximately 6.5-mm diameter holes on 20-mm centers,

over a minimum central area of 350 by 350 mm.

96.2 A ﬂat circular indentor that exerts a force of 750 6 20

N on the test specimen at maximum indentation. The indentor

shall have an overall diameter of 250 6 1 mm with a 25 6

1-mm radius at the lower edge, to prevent cutting hard foam.

96.3 By means of a crank or other suitable mechanism, the

machine shall be capable of oscillating either the platen

carrying the test specimen or the indentor support mounting

towards each other in a vertical direction at a frequency of 70

6 5 cycles per minute. For Procedure C the frequency shall be

10 6 1 cycles per minute.

96.4 The indentor shall be free to be lifted in its mounting to

prevent overloading of the test specimen.5

97. Test Specimen

97.1 The test specimen shall be 380 by 380 by 50 mm. One

specimen shall be tested, unless otherwise agreed upon by the

supplier and the purchaser.

98. Initial Measurement

98.1 The specimen shall be conditioned for at least 12 h and

also fatigued at 23 6 2°C and 50 6 5 % relative humidity.

98.2 Measure the 40 % IFD of the test specimen in accor-

dance with Sections 16-22. Measure the original thickness with

4.5-N contact force after preﬂexing.

99. Procedure

99.1 Mount the specimen on the base platen. Set the counter

to zero, start the machine, and fatigue the test specimen for

5

where:

Ft = loss in thickness, %,

to = original specimen thickness, and

tf = ﬁnal specimen thickness.

101.3 Calculate the percent loss of force deﬂection, as

follows:

FL 5

~Fo 2 Ff !

3 100

F~Lo !

(11)

where:

FL = loss of 40 % indentation force deﬂection, %,

Fo = original 40 % indentation force deﬂection value, and

Ff = ﬁnal indentation force deﬂection value.

102. Report

102.1 Report the following information:

102.1.1 Percent change in thickness and the percent change

in 40 % IFD if the thickness change is less than 10 %, and

102.1.2 Results of visual examination.

102.1.3 Recovery time whether 60 min or 24 h.

103. Precision and Bias

103.1 See Section 137 for Precision and Bias statements. A

round robin for Procedure C is being planned and the data will

be available by the end of 2006.

TEST I4 —DYNAMIC FATIGUE TEST FOR CARPET

CUSHION

104. Scope

104.1 The purpose of this test is to determine: (1) retention

of load bearing (65 % IFD), (2) a loss in thickness, and (3)

structural breakdown as addressed by visual inspection.

104.2 This procedure describes tests that evaluate the speci-

men by repeatedly deﬂecting the carpet cushion by a 152 mm

12

Detailed drawings are available from ASTM Headquarters. Request Adjunct

ADJD3574.

D 3574 – 05

diameter and 152 mm wide rubber covered roller exerting a

force of 266 6 5N on the test specimens.

104.3 This fatigue test may be conducted by either Proce-

dure A or Procedure B. The test procedures differ only in the

number of cycles used. Procedure A shall use 8000 cycles

(approximately 5 h) and Procedure B shall use 40 000 cycles

(approximately 12 h).

NOTE 26—No similar ISO standard exists.

areas. Set the counter for zero, start the machine, and fatigue

the sample for 40 000 cycles.

109. Final Measurements

109.1 Within 60 6 5 min after the fatigue test is completed

measure the ﬁnal thickness, tf, in accordance with Section 8

and the ﬁnal 65 % IFD, Ff, in accordance with 107.1 using the

original thickness, to, to determine the 65 % IFD deﬂection.

109.2 For a measurement of more permanent fatigue repeat

109.1, except allow 24 6 1h of recovery rather than 60 min.

110. Calculation and Inspection

110.1 Check the specimen for physical breakdown by visual

examination.

110.2 Calculate and report the percentage loss in thickness

as follows:

Fl 5

~to 2 tf !

3 100

~to !

105. Apparatus (Appendix X2)

105.1 The apparatus is identical to that described in Section

87 with the following changes. The roller described in 104.2

replaces the longer roller and is attached perpendicularly. The

base platen is replaced or covered with a 19 mm thick plywood

for mounting the sample. The sample is secured with ﬂoor

tacks or staples. (See Fig. 4 for test apparatus.)

106. Test Specimens

106.1 The specimen is 380 mm long and 230 mm wide and

13 mm thick, unless otherwise agreed upon by supplier and

purchaser.

107. Initial Measurements

107.1 Condition the specimens as in Section 6. The test

should be run under the same conditions, if possible. Preﬂex

the specimens two times 75 % of the nominal thickness. After

a 6 6 1 min rest, measure the original thickness, to, in

accordance with Section 8 and determine the original 65 %

IFD, Fo, in accordance with Sections 16-22 using a 102 mm

diameter ﬂat circular indentor foot.

108. Procedure

108.1 Secure the sample to the plywood base using staples

or tape, making sure that the roller will not roll over the stapled

(12)

where:

Fl = loss in thickness, %,

to = original specimen thickness, and

tf = ﬁnal specimen thickness.

110.3 Calculate the percentage IFD retention as follows:

R 5 100 2

~Fo 2 Ff 3 100!

~Fo!

(13)

where:

R= retain IFD, %,

Lo = original IFD force, and

Lf = ﬁnal IFD force.

FIG. 4 Three-station Carpet Cushion Fatigue Tester

13

D 3574 – 05

111. Report

111.1 Report the following information:

111.1.1 Percentage loss in thickness and percentage reten-

tion of 65 % indentation force deﬂection, and

111.1.2 Recovery time whether 60 min or 24 h.

112. Precision and Bias

112.1 Round robin testing to determine the precision of this

method is being planned and the data will be available by the

end of 2006.

TEST J—STEAM AUTOCLAVE AGING

113. Scope

113.1 This test consists of treating the foam specimen in a

low-pressure steam autoclave and observing the effects on the

properties of the foam specimen. Use either of the following

procedures, J1 or J2 :

113.1.1 Procedure J1, 3 h at 105 6 3°C.

113.1.2 Procedure J2, 5 h at 120 6 5°C.

NOTE 27—ISO 2440 is a similar standard, but there are some technical

differences.

where:

Po = mean property of the unexposed specimen, and

Pf = mean property of the exposed specimen.

117. Report

117.1 Report the following information:

117.1.1 Percent change in physical property,

117.1.2 Test procedure J1 or J2.

118. Precision and Bias

118.1 The precision of this method is dependent on the

material property that is being measured.

TEST K—DRY HEAT AGING

119. Scope

119.1 This test consists of exposing foam specimens in an

air-circulating oven and observing the effect on the properties

of the foam.

NOTE 29—ISO 2440 is a similar standard, but there are some technical

differences.

114. Apparatus

114.1 Steam Autoclave, or similar vessel, that is thermostati-

cally controlled to 62°C and capable of withstanding gage

pressures of up to 140 kPa.

115. Procedure

115.1 Fill the autoclave with fresh-distilled water to a level

50 mm above the bottom of the autoclave. Set the thermostat

control at the desired procedures of test, which is between 105

6 3°C or 120 6 5°C. Allow the autoclave to heat until the

water boils. Place the specimen on edge on a rack in the inside

container so that one specimen does not touch another or any

metal except at the supporting surface. Place the container

inside the autoclave and close and tighten the top. Leave the

safety valve open until all the air is out of the autoclave. This

is apparent when steam begins blowing out of the ports on the

safety valve. Close the valve 2 min after the appearance of

steam, and take the zero time of the heat at this point.

115.2 After the exposed period, turn off the heat, release the

steam pressure, and remove the specimens without delay. Dry

the specimens for 3 h for each 25 mm of thickness at 100 6

5°C in a mechanically convected dry-air oven. Allow them to

come to temperature equilibrium, after removal from the oven,

for at least 2 h at 23 6 2°C and 50 6 5 % relative humidity.

115.3 Test each specimen for the prescribed property in

accordance with the appropriate test method.

NOTE 28—A drying temperature of 70°C may be used where 100°C

adversely affects the ﬁnal properties upon agreement by customer and

supplier.

120. Apparatus

120.1 Air-Circulating Oven, capable of maintaining 140 6

2°C for exposing the specimens. A device for sensing and

recording the temperature of the oven at least every 2 h shall be

attached.

121. Procedure

121.1 Expose the specimens for 22 h at 140 6 2°C. Obtain

and record the oven temperature near the specimen at least

every 2 h.

121.2 Remove the specimens from the oven and condition

for not less than 2 h at 23 6 2°C and 50 6 5 % relative

humidity.

122. Calculation

122.1 Calculate the percent change in physical property as

follows:

Physical property change, % 5

~~Po 2 Pf!!

3 100

~Po !

(15)

where:

Po = mean property of the unexposed specimen, and

Pf = mean property of the exposed specimen.

123. Report

123.1 Report the following information:

123.1.1 Percent change in physical property.

124. Precision and Bias

124.1 The precision of this method is dependent on the

material property that is being measured.

TEST L—WET HEAT AGING

125. Scope

125.1 This test consists of exposing foam specimens in an

environmental chamber and observing the effect on the prop-

erties of the foam.

14

116. Calculation

116.1 Calculate the present change in physical property as

follows:

Physical property change, % 5

~Po 2 Pf!

3 100

~Po !

(14)

D 3574 – 05

NOTE 30—There is no similar or equivalent ISO standard.

134. Procedure

134.1 Place the test specimen on the perforated supporting

plate. Bring the indenter foot into contact with the specimen

with a 4.5 N preload to determine the specimen’s initial

thickness. Immediately indent the specimen 75 % of its initial

thickness at a speed of 1000 6 100 mm/min. After a 60-s dwell

time, return the indenter to a 5 % deﬂection at 1000 6 100

mm/min, starting a stopwatch immediately upon initiating the

upward movement of the indenter. Stop the watch as soon as

the foam recovers to a 4.5 N preload on the indenter.

135. Report

135.1 Report the recovery time in seconds.

136. Precision and Bias

136.1 A round robin is being planned to determine the

precision of this test method and the data shall be available by

the end of 2006. In a single lab repeatability study performed

in 2005 with two materials, the recovery times varied by 8.2 %

and 15.9 %, respectively.

137. Precision and Bias

137.1 Precision and bias for test methods in this standard

are based on round robin studies conducted by the Polyure-

thane Foam Association from 1998 to 2000 in accordance with

Practice E 691. The Test B2 data was generated by the molded

foam industry in 2004. For each study, three or four materials

were carefully selected to cover the range of properties

expected in commercially available products. The number of

labs varied from 6 to 10. The samples were distributed by one

lab, but individual specimens were prepared at the labs

performing the tests. Each laboratory obtained six test results

for each material. Precision, characterized by repeatability (Sr

and r) and reproducibility (SR and R) have been determined as

shown in the individual tables.

137.2 Bias—There are no recognized standards by which to

estimate bias for these test methods. (Warning—The explana-

tion of r and R are only intended to present a meaningful way

of considering the approximate precision of these test methods.

The data in the tables should not be applied to acceptance or

rejection of materials, as these data apply only to the materials

tested in the round robins and are unlikely to be rigorously

representative of other lots, formulations, conditions, materials,

or laboratories. Users of these test methods should apply the

principles outlined in Practice E 691 to generate data speciﬁc

to their materials and laboratory.)

NOTE 32—The precision data presented in the tables were obtained

using the test conditions deﬁned in the test methods. If a material

speciﬁcation deﬁnes other test conditions, these precision data shall be

assumed not to apply.

126. Apparatus

126.1 Environmental Chamber, capable of maintaining 50

6 2°C and 95 6 5 % RH for exposing the specimens. A device

for sensing and recording the temperature of the oven at least

every 2 h shall be attached.

NOTE 31—Other temperature and humidity conditions may be used as

agreed upon by the purchaser and the supplier.

127. Procedure

127.1 Place the specimens into the environmental chamber

set to the temperature and humidity conditions speciﬁed in

126.1, making sure they do not touch each other. For tests such

as compression set the specimens shall be clamped into the test

ﬁxture before putting them into the chamber. Expose the

specimens for 22 h 6 5 min or as agreed upon by the supplier

and purchaser.

127.2 After the exposure period remove the specimens from

the oven and from any ﬁxturing and then condition them for

not less than 2 h at 23 6 2°C and 50 6 5 % relative humidity

or as speciﬁed in the test method being evaluated.

127.3 Perform any measurements and calculations speciﬁed

in the test method being evaluated.

128. Calculation

128.1 Calculate the percent change in physical property as

follows:

Physical property change, % 5

@~Po 2 Pf!#

3 100

~Po!

(16)

where

Po = mean property of the unexposed specimen, and

Pf = mean property of the exposed specimen.

129. Report

129.1 Report the following information:

129.1.1 Percent change in physical property, and

129.1.2 Test method evaluated.

130. Precision and Bias

130.1 The precision of this method is dependent on the

material property that is being measured.

TEST M—RECOVERY TIME

131. Scope

131.1 This method is used to determine the recovery time of

slow recovery (viscoelastic) foams.

132. Apparatus

132.1 Use the standard IFD apparatus as described in 17.1.

133. Test Specimen

133.1 Use the standard IFD specimen as described in 18.1.

One specimen shall be tested, unless otherwise agreed upon by

supplier and purchaser.

138. Keywords

138.1 bonded; ﬂexible cellular; molded; slab; urethane

15

D 3574 – 05

TABLE 1 Density Test A, kg/m3

(8 Laboratories)

Material

1

2

3

A

TABLE 4 IFD Test B1, 65 % IFD, N

(8 Laboratories)

r

C

Avg.

27.21

43.44

35.07

Sr

A

SRB

0.31

0.34

0.61

R

D

Material

1

2

3

A

Avg.

147.91

253.33

491.16

SrA

2.99

2.34

7.18

SRB

5.68

8.49

20.64

rC

8.37

6.56

20.16

RD

15.92

23.77

57.81

0.23

0.28

0.51

0.64

0.78

1.43

0.88

0.94

1.70

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 2 IFD Test B1, Thickness, mm

(8 Laboratories)

Material

1

2

3

A

TABLE 5 IFD Test B1, 25 % RT IFD, N

(8 Laboratories)

RD

1.50

1.52

2.08

A

Avg.

104.1

102.3

99.1

SrA

0.20

0.28

0.45

SRB

0.31

0.34

0.61

rC

0.53

0.53

0.74

Material

1

2

3

Avg.

58.23

99.83

145.14

SrA

0.83

0.94

2.53

S RB

1.26

2.14

2.53

rC

2.33

2.64

4.62

RD

3.54

5.99

11.12

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 3 IFD Test B1, 25 % IFD, N

(8 Laboratories)

Material

1

2

3

A

TABLE 6 IRGL Test B2, 4.5 N Height, mm

(8 Laboratories)

RD

5.85

12.06

24.44

A

Avg.

73.48

136.35

249.11

SrA

0.93

1.10

3.16

SRB

2.09

4.31

8.73

rC

2.62

3.07

8.85

Material

1

2

3

4

Avg.

99.84

100.69

101.51

100.59

SrA

0.38

1.04

0.90

0.61

SRB

0.73

1.04

1.00

1.06

rC

1.06

2.91

2.51

1.71

RD

2.04

2.91

2.79

2.97

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

16

D 3574 – 05

TABLE 7 IRGL Test B2, 110 N Height, mm

(8 Laboratories)

Material

1

2

3

4

A

TABLE 11 Compression Set Test D, 90 % Cd, %

(9 Laboratories)

R

D

Avg.

87.05

99.07

99.79

99.49

Sr

A

SR

B

r

C

Material

1

2

3

A

Avg.

3.72

6.45

9.07

SrA

0.68

0.79

0.92

SRB

0.92

1.11

1.78

rC

1.91

2.22

2.59

RD

2.58

3.11

5.00

2.25

1.00

0.88

0.63

5.03

1.00

1.01

1.06

6.31

2.79

2.47

1.76

14.07

2.79

2.83

2.96

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 12 Tensile Test E, D 3574 Die, kPa

TABLE 8 IRGL Test B2, 220 N Height, mm

(8 Laboratories)

Material

1

2

3

4

A

(10 Laboratories)

Material

Avg.

45.84

74.96

91.62

SrA

1.54

3.02

4.02

SRB

2.82

4.56

5.11

rC

4.33

8.47

11.24

RD

7.90

12.78

14.32

R

D

Avg.

41.06

93.76

98.37

98.66

Sr

A

SR

B

r

C

2.82

0.98

0.92

0.58

5.20

3.54

1.26

1.06

7.88

2.74

2.57

1.62

14.55

9.92

3.53

2.98

1

2

3

A

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 13 Tensile Test E, D 412 Die, kPa

(10 Laboratories)

Material

Avg.

46.06

78.20

89.99

SrA

2.67

3.88

3.26

S RB

4.00

4.81

3.42

rC

7.48

10.85

9.12

RD

11.19

13.47

9.56

TABLE 9 CFD Test C, 50 % CFD, kPa

(9 Laboratories)

Material

1

2

3

A

Avg.

2.06

3.04

9.36

SrA

0.05

0.07

0.14

SRB

0.29

0.58

0.38

rC

0.14

0.18

0.40

RD

0.81

1.62

1.07

1

2

3

A

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 14 Tensile Test E, Elongation by Crosshead Travel, D 412

Die, %

(10 Laboratories)

Material

Avg.

218.4

231.8

154.5

SrA

16.2

15.4

14.1

S RB

24.2

24.9

27.5

rC

45.5

43.0

39.4

RD

67.6

69.6

77.1

TABLE 10 Compression Set Test D, 90 % Ct, %

(9 Laboratories)

Material

1

2

3

A

Avg.

3.36

5.78

8.23

SrA

0.62

0.82

0.83

SRB

0.83

0.97

1.61

rC

1.73

2.30

2.34

RD

2.34

2.71

4.51

1

2

3

A

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

17

D 3574 – 05

TABLE 15 Tensile Test E, Elongation by Crosshead Travel,

D 3574 Die, %

(10 Laboratories)

Material

1

2

3

A

TABLE 19 Resilience Test H, %

(8 Laboratories)

Material

Avg.

46.1

70.8

69.2

SrA

0.82

1.00

0.99

SRB

2.86

3.15

2.89

rC

2.31

2.79

2.76

RD

8.00

8.82

8.09

Avg.

205.3

219.2

146.4

SrA

13.2

15.2

14.2

SRB

23.6

24.0

26.3

rC

36.9

42.6

39.7

RD

66.0

67.2

73.6

1

2

3

A

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 20 Pounding Fatigue Test I3 1 h Thickness Loss, %

TABLE 16 Tensile Test E, Elongation by Benchmarking, D 3574

Die, %

(10 Laboratories)

Material

1

2

3

Avg.

217.9

236.6

158.9

SrA

12.1

14.6

16.9

SRB

30.2

30.3

31.9

rC

33.9

40.7

47.3

RD

84.5

84.9

89.2

A

(7 Laboratories)

Material

1

2

3

Avg.

1.69

1.46

2.50

SrA

0.76

0.39

0.24

SRB

0.87

0.42

0.61

rC

2.14

1.08

0.68

RD

2.43

1.17

1.70

ASr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 21 Pounding Fatigue Test I3 24 h Thickness Loss, %

(7 Laboratories)

Material

Avg.

1.47

1.11

1.81

SrA

0.70

0.32

0.24

SRB

0.97

0.39

0.52

rC

1.96

0.89

0.68

RD

2.70

1.10

1.47

TABLE 17 Tear Test F, N/m

(6 Laboratories)

Material

1

2

3

A

Avg.

599.4

244.0

215.2

SrA

41.6

18.0

17.6

SRB

52.1

35.3

28.3

rC

116.5

50.4

49.2

RD

145.8

98.9

79.1

A

1

2

3

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

TABLE 22 Pounding Fatigue Test I3 1 h 40 % IFD Loss, %

(7 Laboratories)

Material

Avg.

29.9

20.6

34.1

SrA

1.34

2.11

1.56

SRB

2.93

2.49

2.86

rC

3.75

5.92

4.36

RD

8.22

6.96

8.01

TABLE 18 Air Flow Test G, m3/min

(7 Laboratories)

Material

1

2

3

A

Avg.

0.056

0.109

0.160

SrA

0.002

0.004

0.009

SRB

0.006

0.013

0.024

rC

0.006

0.011

0.027

RD

0.017

0.038

0.068

A

1

2

3

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

18

D 3574 – 05

TABLE 23 Pounding Fatigue Test I3 24 h 40 % IFD Loss, %

(7 Laboratories)

Material

1

2

3

A

Avg.

24.3

17.2

27.0

SrA

2.46

2.09

1.95

SRB

3.26

2.53

3.56

rC

6.88

5.86

5.46

RD

9.14

7.09

9.96

Sr = within-laboratory standard deviation for the indicated material. It is ob-

tained by pooling the within-laboratory standard deviations of the test results from

all of the participating laboratories.

BSR = between-laboratory reproducibility, expressed as standard deviation.

Cr = within-laboratory critical interval between two results = 2.8 3 Sr.

DR = between-laboratories critical interval between two results = 2.8 3 SR.

APPENDIXES

(Nonmandatory Information)

X1. SUGGESTED METHOD FOR SPECIFYING FLEXIBLE URETHANE FOAMS

X1.1 For simpliﬁcation in specifying foams, a line call out

system may be used. The line call out could be used on

engineering drawings for parts. The properties correspond to

the sections of this test method. The call out format shall be as

follows:

ASTM D 3574 Type [Slab, Molded, Bonded or other, as speciﬁed]

Coring [Cored or Uncored]

Urethane Chemistry [Polyether, Polyester, HR, Conventional]

A Density [kg/m3] maximum, minimum or range

B1 IFD [N] [for 25 % and 65 % deﬂections, 100 mm thick sample] max, min, or range

B2 IRGL [mm] [at 4.5, 110 and 220 N, 100 mm thick sample] max, min, or range

C CFD [kPa] [50 % deﬂection] max, min, or range

D Compression set [%] [method—Cd or Ct] max

E Tensile [kPa] min

F Tear [N/m] min

G Air Flow [cfm] min

H Ball Rebound [%] min

I1 Static Fatigue [percent thickness loss and 25 % and 65 % IFD loss] max

I2 Roller Shear [percent loss of thickness and IRGL values] max

I3 Constant Force Pounding [percent change in thickness and percent change in 40 % IFD] max

I4 Dynamic Fatigue Test for Carpet Cushion [percent loss of thickness and percent retention of 65 % IFD value] maximum value and minimum value, respectively

J1 Steam Autoclave [physical properties to be tested as (tests A through I or M as speciﬁed, units as above] maximum or minimum values based on test speciﬁed

J2 Steam Autoclave [physical properties to be tested as (tests A through I or M as speciﬁed, units as above] maximum or minimum values based on test speciﬁed

K Dry Heat Aging [physical properties to be tested as (tests A through I or M as speciﬁed, units as above] maximum or minimum values based on test speciﬁed

L Wet Heat Aging [physical properties to be tested as (tests A through I or M as speciﬁed, units as above] maximum or minimum values based on test speciﬁed

M Recovery Time [seconds] max, min, or range

X Other tests as speciﬁed (Individual tests listed with subscripts)

X1.2 Example:

D 3574 Type [Slab]

Coring [Uncored]

Urethane Chemistry [Polyether]

A Density [15.5 kg/m3] min

B1 IFD [13 mm thick specimen 80-140 N ] range

C CFD [3.0-4.0 kPa at 50 % deﬂection] range

D Compression Set [10 % Ct] maximum

E Tensile [80 kPa] min

F Tear [0.25 kN/m] min

J1 Steam Autoclave [15 % change in CFD] max

K Dry Heat Aging [15 % change in CFD] max

X1 Flammability—MVSS 302 [102 mm/min] max

X2 Odor—SAE J 1351 [3] max

X3 Stain Resistance—ASTM D 925 Test A [no staining]

X4 Low Temperature Flexibility—DCX MSAY 349 [no rupturing]

X5 No auxiliary blowing agents may be used to manufacture product

19

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

X2. SUGGESTED METHOD OF CONSTRUCTION FOR A ROLLER SHEAR

DYNAMIC FLEX FATIGUE APPARATUS

X2.1 The following requirements are established to deﬁne

the equipment and relationship of parts for a constant-load

roller shear machine. See Fig. X2.1 and Fig. X2.2 for reference

to part numbers.

X2.2 Roller, 1:

X2.2.1 Dimensions—457-mm minimum length, and 76.20

6 1.27-mm diameter.

X2.2.2 Material—Corrosion and wear-resistant metal, ei-

ther (1) chrome-plated material, or (2) stainless steel.

X2.2.3 Surface Finish—Finish surface on roller is to be

ground and equivalent to at least 0.001 mm.

X2.2.4 The mass of the roller shall not exceed 11.340 kg.

X2.3 Roller Mounting Bracket Assembly 2, 3, 4, 11—The

assembly consists of metal members designed to attach the

roller to a pivot point, to provide bearing surfaces for minimum

friction for turning, and to serve as a platform to add required

mass to the roller.

X2.3.1 Bearings, 2 and 4—The proper bearings are required

on each end or roller axis (A-A) and also on the pivot axis

(B-B). The bearing should be equivalent to the following

example:

Bearing No. 4—Nice No. 1635, DC Ball Bearing 19 by 32 by

13 mm.

Bearing No. 2—Nice No. 6906, ﬂange mounted radial bearing.

NOTE X2.1—Roller axis bearings may be mounted in the bracket with

the axle attached to the roller or, if the roller is a hollow cylinder, the

bearing may be press ﬁt into the cylinder end with the bracket furnishing

the axle.

X2.3.2 Pivot Arm, 11—The distance between the pivot axis

and the roller axis shall be 203.20 6 6.35 mm.

X2.3.3 Roller Bracket Connector, 3, connects the right and

left bearing brackets across the top of the roller. The connection

must also provide a ﬂat horizontal surface with means (pin) to

attach the weights. The weights must be centered directly

above the axis of the roller.

X2.3.4 Axis Relationship—The roller axis (A-A) and pivot

axis (B-B) must be parallel and lie in the same horizontal plane

parallel to the specimen mounting base.

X2.3.5 Alignment and Clearance—Brackets and axles must

be aligned so that no binding occurs to obstruct free turning on

either axis. Brackets and other support members (5) must give

free clearance so that specimen is not touched during test other

than by roller surface.

X2.3.6 Weight, 6—The total vertical force exerted by the

assembly plus the roller should not exceed 111 N as measured

at a point directly above or below the roller axis when both

roller and pivot axes are in the same horizontal plane (X2.3.4).

Additional weights to be added as shown.

X2.3.7 Vertical Adjustment, 7—If the roller is not driven to

provide stroke movement, provision should be made so that

FIG. X2.1 Roller Shear Machine—Top View

20

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

FIG. X2.2 Roller Shear Machine—Side View

attachment of the pivot axis to the support can be raised or

lowered at least 75 mm [3 in.]. This adjustment must be able to

be made in not less than 12.5-mm increments.

X2.4 Specimen Mounting Base, 8:

X2.4.1 Dimensions—500-mm minimum length. 500-mm

minimum width, and 9.5-mm minimum thickness.

X2.4.2 Material—Structural-grade carbon steel.

X2.4.3 Perforation—6-mm diameter holes on 20-mm cen-

ters, over a minimum area covering 350 mm in length by 350

mm in width.

X2.4.4 Surface Finish—Top surface shall be a ﬁnish grind.

X2.4.5 Hold-Down Plates, 9—Provision to attach metal or

wood hold-down plates for clamping cotton sheeting retaining

strips to base. Four plates are required to cover perimeter of

specimen size.

X2.4.6 Vertical Adjustment and Level, 10—If mounting

base is not driven to provide stroke movement, provision

should be made for vertical adjustment of at least 75 mm. This

adjustment must be able to provide vertical movement in not

less than 12.5-mm increments and maintain a horizontal level

condition of the mounting base.

X2.5 Mechanical Requirements:

X2.5.1 Stroke Length—The length of stroke shall be 330 6

12 mm.

X2.5.2 Stroke Speed, Stroke Drive—The rate of stroke

speed should produce 0.47 6 0.03 Hz. A cycle is a complete

forward and reverse stroke. Either the roller or the mounting

base may be driven to produce stroke travel. In either case, the

drive mechanism must produce travel in a horizontal plane.

X2.5.3 Angular Offset—The axis of the roller should be

level and mounted at a 15 6 3° offset from perpendicular to the

direction of the stroke.

X2.5.4 Mounting Base Location—The length of the mount-

ing base should be parallel to the direction of the stroke and

centered under the midpoint of the stroke and the center of the

roller. The distance of the base surface from the roller axis

(X2.3.4) should be 45 mm when vertical adjustment provides

a minimum clearance.

X2.5.5 Cycle Counter—Means to record the number of

cycles should be provided.

X3. DEFINITIONS OF TERMS USED TO DESCRIBE THE FORCE-DEFLECTION CURVE

OF FLEXIBLE URETHANE FOAM

X3.1 support factor—the ratio of the 65 % indentation

force deﬂection to the 25 % indentation force deﬂection

determined after 1 min of rest. Most speciﬁcations are based on

the 25 % IFD value of a 100-mm foam. The support factor thus

indicates what 65 % IFD value would be acceptable for a

particular application. The 65 % IFD measures the support

region of the stress-strain curve. Seating foams with low

support factors will usually bottom out and give inferior

performance.

Support factor ~SF! 5 ~65 % IFD/25 % IFD!

(X3.1)

Synonyms—Sag factor, hardness ratio, comfort factor. These

terms should be removed from the vocabulary. Support factor

is the term of choice.

X3.2 guide factor—the ratio of the 25 % indentation force

deﬂection to the density after a 1-min rest. Most speciﬁcations

do not have a density requirement; therefore the product with

the highest guide factor has the cost advantage but not

necessarily the performance advantage.

Guide factor ~GF! 5 ~25 % IFD/density!

(X3.2)

21

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

X3.3 initial hardness factor—the ratio of the 25 % inden-

tation force deﬂection force to the 5 % indentation force

deﬂection determined without the 1-min rest. The initial

hardness ratio deﬁnes the surface feel of a ﬂexible urethane

foam. Supple or soft surface foam will have a high value, while

boardy or stiff surface foams will have a low value (Note

X3.1).

Initial hardness factor ~IHF! 5 ~25 % IFD/5 % IFD!

(X3.3)

Synonym— Comfort factor.

NOTE X3.1—Standard IFD curves can be used to generate the IHF, IM,

and MIF data.

X3.4 hardness index—the term used in some speciﬁcations

for the 50 % IFD value. The chair designer will often design

furniture for a maximum 50 % indentation. Bar stools on the

other hand may be designed for only a 20 % deﬂection.

X3.5 indentation modulus—the force required to produce

an indentation of an additional 1 % between the limits of 20 %

indentation force deﬂection and 40 % indentation force deﬂec-

tion determined without the 1-min rest. The slope of this line

depends upon the resistance of the cells struts to post buckling

(Note X3.1).

Indentation modulus ~IM! 5 ~40 % IFD 2 20 % IFD/20 % IFD!

(X3.4)

FIG. X3.1 Indentation Stress-Strain Curve (MIF is Zero)

FIG. X3.2 Indentation Stress-Strain Curve (MIF is positive)

X3.6 modulus irregularity factor—the intercept produced

on the stress axis by extrapolation of the linear portion of the

stress-strain curve. The indentation modulus, that is, the slope

of the line, may be substantially constant up to and beyond the

40 % indentation level. In this event, the indentation stress-

strain curve is linear and passes through the origin Fig. X3.1.

The indentation modulus usually varies at low levels of strain

before reaching a constant value at above approximately 10 per

strain. The stress-strain curve may exhibit a marked step in that

region which may result in some discomfort in seating appli-

cations, Fig. X3.2 and Fig. X3.3. The MIF value is calculated

from the same data necessary to derive the modulus of the

foam as a seating material (Note X3.1).

Modulus irregularity factor ~MIF! 5 2 3 20 % IFD 2 40 % IFD

(X3.5)

22

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

FIG. X3.3 Indentation Stress-Strain Curve (MIF is negative)

X4. SUGGESTED TESTS FOR DETERMINING COMBUSTIBILITY OF FLEXIBLE URETHANE FOAM

X4.1 This appendix lists for informational purposes only

the test methods commonly used for determining the combus-

tion properties of ﬂexible urethane foams. These tests have

been found useful in ascertaining the effectiveness of additives

and reactants to modify the combustion characteristics of these

materials. See 1.3.

X4.2 Some Applicable Codes and Regulations for Speciﬁed

Applications:

Application

Automotive

Mattress and cushion

Mattress and cushion

Mattress and cushion

Mattress and cushion

Mattress and cushion

Mattress and cushion

Mattress and cushion

Aviation

Aviation

Carpet cushion

Carpet cushion

Miscellaneous

_______________

A

Regulation

DOT MVSS 302

DOC FF 4-72

CAL TB 117

CAL TB 133A

CAL AB 603A

NFPA 260A

NFPA 261A

BSI 5852A

FAA Part 25.853 Par (b) App F

FAA Oil Burner Test

ASTM E84

DOC FFI-70 (Pill Test)

ASTM D 3675

Various governmental bodies have issued regulations based

on Test Methods E 162 and E 662. The regulations are not the

same for all bodies issuing them. Hence, the regulation of the

government having jurisdiction should be consulted.

These standards are used to measure and describe the

response of materials, products, or assemblies to heat and ﬂame

under controlled conditions, but do not by themselves incor-

porate all factors required for ﬁre hazard or ﬁre risk assessment

of the materials, products, or assemblies under actual ﬁre

conditions.

X4.2.1 Sources:

Superintendent of Documents, US Gov-

ernment Printing Office, Washington,

DC 20402

CaliforniaCalifornia Bureau of Home Furnishings,

3485 Orange Grove Ave., North High-

lands, CA 95660

National Fire Protection Association 1 Batterymarch Park, P.O. Box 9101,

Quincy, MA 02269

British StandardBritish Standards Institute, 2 Park Street,

London, England W1A 2B5

Government Documents

Composite test. Foam, fabric, and other components may have a synergistic

effect on each other.

23

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

X5. SUGGESTED METHOD FOR THE VERIFICATION OF AN INCLINED OIL MANOMETER

X5.1 Adjust the feet to level the manometer. With a height

gage resting on a level and ﬂat surface measure the distance to

the top of the glass tube at each major mark. Determine the

area of the tube by direct measurement. The area of the

reservoir is calculated by adding a measured amount of ﬂuid

with both ends of the manometer at atmospheric pressure. The

calculation for the area of the reservoir (A):

A 5 ~v 2 ay!/h

(X5.1)

X5.2 Change in pressure is calculated by:

Pm 2 Pn 5 wy ~sin u 1 a/A!

(X5.2)

where:

v = the

a = the

y = the

h = the

volume added,

area of the inside of the tube,

distance between readings, and

change in height.

where:

Pm =

Pn =

w=

y=

u=

a=

A=

the

the

the

the

the

the

the

low reading,

high reading,

speciﬁc gravity of the indicating ﬂuid,

distance between readings,

angle of the tube to normal,

area of the inside of the tube, and

area of the reservoir.

X5.3 The error is the difference between the calculated and

the indicated value.

X6. SUGGESTED METHOD FOR MEASURING THE HYSTERESIS LOSS OF FOAMS

X6.1 Hysteresis Loss for the purpose of this method is

deﬁned as the difference between the loading energy and the

unloading energy expressed as a percentage of the loading

energy.

Hysteresis Loss 5 [Loading Energy – Unloading Energy]

3 100/[Loading Energy]

where:

indent the sample at a rate of 50 6 5 mm/min by 75 6 5 % of

its original height. Immediately remove the indentation force at

50 6 5 mm/min until the platen fully returns. Calculate the

hysteresis loss as deﬁned above.

Procedure B—CFD Hysteresis Loss

X6.3 Prepare and preﬂex samples in accordance with

ASTM D 3574 Test C. After the 6 6 1 minute waiting period,

compress the sample at a rate of 50 6 5 mm/min by 75 6 5 %

of its original height. Immediately remove the compression

force at 50 6 5 mm/min until the platen fully returns. Calculate

the hysteresis loss as deﬁned above.

NOTE X6.1—Different wait times, test speeds, and deﬂections may be

agreed upon by customer and supplier.

NOTE X6.2—It is extremely important that the Universal Testing

Machine’s (UTM) crosshead reverses direction with minimal hesitation at

the maximum compression point, otherwise false readings will be ob-

tained.

NOTE X6.3—In addition to the hysteresis loss number, identify the

foam as core or with skin, indicate which procedure was followed and any

variances to the procedure, such as those listed in Note X6.1 above.

1) Energy is deﬁned as the area under the Force/Deﬂection

Curve.

2) Loading Energy is the energy required to indent or

compress a ﬂexible material to a preset deﬂection (compression

cycle).

3) Unloading Energy is the Energy recovered when the

indentation or compression platen is retacted from the preset

deﬂection and completely unloaded. (decompression cycle).

Procedure A—IFD Hysteresis Loss

X6.2 Prepare and preﬂex samples in accordance with

ASTM D 3574 Test B1. After the 6 6 1 minute waiting period,

24

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758

D 3574 – 05

FIG. X6.1 Hysteresis Loss

SUMMARY OF CHANGES

Committee D20 has identiﬁed the location of selected changes to this standard since the last issue,

D 3574 - 03, that may impact the use of this standard. (July 1, 2005)

(1) Added Precision and Bias, as well as changed the name for

Test B2: Indentation Residual Gage Load.

(2) Added a standard recovery test for slow recovery foams.

(3) Added a standard hysteresis loss method for urethane

foams.

(4) Added a line call out system for ﬂexible urethane foams.

(5) Deﬁned viscoelastic foams and test method modiﬁcations

associated with their unique properties.

ASTM International takes no position respecting the validity of any patent rights asserted in connection with any item mentioned

in this standard. Users of this standard are expressly advised that determination of the validity of any such patent rights, and the risk

of infringement of such rights, are entirely their own responsibility.

This standard is subject to revision at any time by the responsible technical committee and must be reviewed every ﬁve years and

if not revised, either reapproved or withdrawn. Your comments are invited either for revision of this standard or for additional standards

and should be addressed to ASTM International Headquarters. Your comments will receive careful consideration at a meeting of the

responsible technical committee, which you may attend. If you feel that your comments have not received a fair hearing you should

make your views known to the ASTM Committee on Standards, at the address shown below.

This standard is copyrighted by ASTM International, 100 Barr Harbor Drive, PO Box C700, West Conshohocken, PA 19428-2959,

United States. Individual reprints (single or multiple copies) of this standard may be obtained by contacting ASTM at the above

address or at 610-832-9585 (phone), 610-832-9555 (fax), or service@astm.org (e-mail); or through the ASTM website

(www.astm.org).

25

长  春  恒  越  电  子  科  技  有  限  公  司

www.jlhykj.com 0431-86796799   www.jlhydz.net 0431-86796758