简要说明：

HRM-45DT电动表面洛氏硬度计是一种通过电动加载、保荷卸荷的半自动测试金属材料表面硬度的洛氏硬度计。具有操作更简便、压痕微小、精度高等特点。

适用范围：

表面淬火钢，铜、铝合金薄板，带钢,硬质合金钢，镀锌，镀铬，镀锡，材料表面热处理和化学表面处理的各种金属材料。

HRM-45DT Motorized Superficial Rockwell Hardness Tester adopts motorized testing method. Its testing force can be loaded, kept and unloaded automatically. Avoid man-made error and easy to use. The characteristics of the instrument is light testing force and therefore, leaving very small indentation.

Usage Range:

Surface hardened steel, copper, aluminum alloy thin sheet, hard alloy steel, zinc layers, chrome layers, tin layers, surface hardened treating and chemical treating materials, etc.

技术数据（Technical Specifications）      HRM-45DT电动表面洛氏硬度计

| 表面洛氏标尺 (Superficial Rockwell Scales) | HR15N, HR30N, HR45N, HR15T, HR30T, HR45T |
| --- | --- |
| 初试验力（Initial Testing Force） | 3Kg(29.42N) |
| 试验力（All Testing Force） | 15Kg(147.1N),30Kg(294.2N),45Kg(441.3N) |
| 硬度读取 (Indication of Hardness Value) | 表盘式（Dial ） |
| 保菏时间(Duration Time) | 2 ~ 60S |
| 试件最大高度 Max. Height of Specimen | 170mm |
| 仪器尺寸(长X宽X高) (Overall Dimension：LXWXH) | 520X240X700MM |
| 仪器重量(Net Weight) | 80 Kg |
| 电源( Power Supply) | AC220V + 5%, 50~60 Hz |
| 执行标准 (Carried Standard) | GB/T230.2 国家标准、JJG112检定规程 GB/T230.2 Chinese Standard and JJG112 Testing Rule |
| 标准配件、附件 (Standard Accessories) | 金刚石洛氏压头，直径1.5875mm硬质合金球压头，大平试抬、中平试台、V型试台，硬度块，电源线等 Diamond Rockwell Indenter, Diameter 1.5875mm Hard Alloy Steel Ball Indenter, Large Testing Table , Medium Testing Table and V-shaped Testing Table,HR30N and HR30T Hardness Blocks , Power Cable, etc. |

本公司现货供应以上型号HRM-45手动表面洛氏硬度计，本公司只销售全新正品，值得您的信赖！

更多产品请访问：www.1718port.com  www.sell17.com

上海麦聚瑞电子仪器有限公司为上海地区的总代理，为您提供完备的售前、售中、及售后服务。欢迎 新老客户来电咨询、洽购。

联系人：景小姐，张先生，包小姐

技  术：晏先生

电话：021-53084218 53084217 53084219 53085318
传真：021-51685888  53084219-110